Maryland Department of Transportation State Highway Administration

Appendix C - Frequency Guide, All Phases

Maryland Department of Transportation

State Highway Administration

# Material Quality Assurance Processes

# Admixtures for Concrete

## Plant or Product Qualification

Evaluation of Production Facility for CTD Materials	Facility Qualification

Production facility data maintained to provide a basis for qualified products.

1  per	1	Prior to Usage on Project

Evaluation of Material Product for CTD Materials	Product Qualification

Qualification of Material Product for use on State Projects.	1  per	1	Prior to Usage on Project

Material Product QC	Product Qualification

Concrete Technology Laboratory to collect and evaluate Admixture Material Samples.

1 Quart in a Screw Top Can

# Aggregate Materials, Controlled Mixtures

1  per	1	Months

## Plant or Product Qualification

Evaluation of Production Facility for SATD Materials	Facility Qualification

Qualification of Production Facility for state projects.

.

1  per	1	Prior to Source Request

1  per	1	Year

Evaluation of Material Product for SATD Materials	Product Qualification

Qualification of Material Product.

35 Lbs, of final mix in a Soils Bag

3  per	1	Prior to Source Request

1  per	2	Year

| Routine SATD Production QA |  |  |  |  | Product QC/QA |
| --- | --- | --- | --- | --- | --- |
| Production Quality Assurance | 1 | per | 20 | Production Day |  |
| . |  |  |  |  |  |
| SATD Material Product QC |  |  |  |  | Product QC/QA |
| Producer to perform daily gradations and moisture checks | 1 | per | 1 | 8 Hour Shift |  |
| on aggregate materials. | 1 | per | 1000 | Ton |  |
| 35 Lbs in a Soils Bag |  |  |  |  |  |

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

Material Verification for SATD Materials	Material Verification

Project Engineer to verify load ticket for correct JMF.	1  per	1	Placement Day

Project Site Testing	Material Sampling and Testing

Compaction and Moisture analysis performed by Project Engineer. Submit compaction report to MMD for clearance.

1  per	1	Placement Day

1  per	1	Lane Mile per Lift

# Aggregate Materials, Crushed Gradations

## Plant or Product Qualification

Evaluation of Production Facility for SATD Materials	Facility Qualification

Evaluation of Crushed Aggregate producers that wish to be placed on the Aggregate Bulletin.

1  per	1	Prior to Usage on Project

1  per	1	Year

Evaluation of Crushed Aggregate producers that do NOT require to be listed in the Aggregate Bulletin.

1  per	1	Prior to Usage on Project

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing

.

1  per	1	Prior to Usage on Project

## Material Production

| SATD Material Review |  |  |  | Material Certification for Project Usage |
| --- | --- | --- | --- | --- |
| Material to be sampled as Common Borrow at its place of origin. Project Engineer to contact SATD to schedule a sampling. | 1 | per | 1 | Prior to Usage on Project |
| 35 LBS in a Soils Bag |  |  |  |  |
| Material to be sampled as Capping Borrow at its place of origin. Project Engineer to contact SATD to schedule a sampling. | 2 | per | 1 | Prior to Usage on Project |
| 35 LBS in a Soils Bag |  |  |  |  |
| Material to be sampled as Modified Borrow at its place of origin. Project Engineer to contact SATD to schedule a sampling. | 2 | per | 1 | Prior to Usage on Project |
| 35 LBS in a Soils Bag |  |  |  |  |
| Material to be sampled as Select Borrow at its place of origin. Project Engineer to contact SATD to schedule a sampling. | 2 | per | 1 | Prior to Usage on Project |
| 35 LBS in a Soils Bag |  |  |  |  |

Project Construction

Material Verification for SATD Materials	Material Verification

Project Engineer to verify material product, submit Form 14.

Project Engineer to submit verification samples of Common Borrow material.

35 LBS in a Soils Bag

Project Engineer to submit verification samples of Modified Borrow material.

35 LBS in a Soils Bag

Project Engineer to submit verification samples of material of Select Borrow.

35 LBS in a Soils Bag

1  per	1	Placement Day

1  per	15000	Cubic Yard

1  per	15000	Cubic Yard

1  per	15000	Cubic Yard

Project Site Testing	Material Sampling and Testing

Compaction and Moisture analysis of Common Borrow to be performed by Project Engineer. Submit Compaction report to MMD for clearance.

35 LBS in a Soils Bag

4  per	1	Lane Mile per Lift

1  per	2000	Cubic Yard

Compaction and Moisture analysis of Capping Borrow to be performed by Project Engineer. Submit Compaction report to MMD for clearance.

35 LBS in a Soils Bag

Compaction and Moisture analysis of Modified Borrow to be performed by Project Engineer. Submit Compaction report to MMD for clearance.

35 LBS. in a Soils Bag

Compaction and Moisture analysis of Select Borrow to be performed by Project Engineer. Submit Compaction report to MMD for clearance.

35 LBS in a Soils Bag

Compaction and Moisture analysis of Select Borrow for Trench Backfill to be performed by Project Engineer.

Submit Compaction report to MMD for clearance.

# Aggregate Materials, High Friction Surf. Treatment

4  per	1	Lane Mile per Lift

1  per	2000	Cubic Yard

4  per	1	Lane Mile per Lift

1  per	2000	Cubic Yard

4  per	1	Lane Mile per Lift

1  per	2000	Cubic Yard

1  per	150	Linear Feet per 3 Foot Lift

## Plant or Product Qualification

Evaluation of Production Facility for SATD Materials	Facility Qualification

1  per	1	Prior to Usage on Project

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

| SATD Certification Review |  |  |  | Material Certification for Project Usage |
| --- | --- | --- | --- | --- |
| Material Certification/Documentation to be provided by material supplier during Source Submission. | 1 | per | 1 | Prior to Usage on Project |
| SATD Material Review |  |  |  | Material Certification for Project Usage |
| Supplier to provide SATD samples of Calcined Bauxite Aggregate 45 days prior to construction. Supplier to contact SATD for delivery instructions. | 2 | per | 1 | Prior to Usage on Project |
| Supplier to provide SATD samples of Polymer Resin Binder. Supplier to contact SATD for delivery instructions | 1 | per | 1 | Prior to Usage on Project |

Project Construction

Material Verification for SATD Materials	Material Verification

Project Engineer to verify the coverage rate of the retained aggregate meets the required quantity of the special provision

Project Engineer to contact the Office of Material Technology to coordinate field acceptance testing (Table 3 of Special Provision) within 60 days after Construction

# Aggregate Materials, Other Stone and Sand

1  per	1	Test Section

1  per	0.1	Lane Mile

## Plant or Product Qualification

Evaluation of Production Facility for SATD Materials	Facility Qualification

Evaluation of Crushed Aggregate producers that wish to be placed on the Aggregate Bulletin.

Evaluation of Crushed Aggregate producers that do NOT require to be listed in the Aggregate Bulletin.

1  per	1	Prior to Usage on Project

1  per	1	Prior to Usage on Project

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

Material Verification for SATD Materials	Material Verification

Project Engineer to verify material, Submit form 14 for clearance

# Aggregate Materials, Recycled PCC Gradations

1  per	1	Item Completion

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing

.

1  per	1	Prior to Source Request

## Material Production

| SATD Certification Review |  |  |  | Material Certification for Project Usage |  |
| --- | --- | --- | --- | --- | --- |
| Material Certification to be provided by material supplier during facility visit. | 1 | per | 1 | Prior to Usage on Project |  |
| . |  |  |  |  |  |
| SATD Material Review |  |  |  | Material Certification for Project Usage |  |
| Material to be sampled as Common Borrow at its place of origin. Project Engineer to contact SATD to schedule a sampling. | 2 | per | 1 | Prior to Usage on Project |  |
| 35 LBS in a Soils Bag |  |  |  |  |  |
| Material to be sampled as Modified Borrow at its place of origin. Project Engineer to contact SATD to schedule a sampling. | 2 | per | 1 | Prior to Usage on Project |  |
| 35 LBS in a Soils Bag |  |  |  |  |  |
| Material to be sampled as Select Borrow at its place of origin. Project Engineer to contact SATD to schedule a sampling. | 2 | per | 1 | Prior to Usage on Project |  |
| 35 LBS in a Soils Bag |  |  |  |  |  |
| Project Construction |  |  |  |  |  |
| Project Sampling and Lab Testing of SATD Material |  |  |  |  | Material Verification |
| Project Engineer to submit verification samples of 1 Common Borrow material. |  | per | 15000 | Cubic Yard |  |
| 35 LBS in a Soils Bag Project Engineer to submit verification samples of material 1 of Modified Borrow. |  | per | 15000 | Cubic Yard |  |
| 35 LBS in a Soils Bag Project Engineer to submit verification samples of Select 1 |  | per | 15000 | Cubic Yard |  |
| Borrow material. |  |  |  |  |  |

35 LBS in a Soils Bag

Project Site Testing	Material Sampling and Testing

Project Engineer to verify pH of placed recycled materials.	1  per	1	Project Completion

Project Engineer to verify pH of placed material, and perform Compaction and Moisture analysis of Common Borrow. Submit Compaction report to MMD for clearance.

4  per	1	Lane Mile per Lift

1  per	2000	Cubic Yard

Project Engineer to verify pH of placed recycled material, and perform Compaction and Moisture analysis of Modified Borrow.

4  per	1	Lane Mile per Lift

1  per	2000	Cubic Yard

Project Engineer to verify pH of placed material, and perform Compaction and Moisture analysis of Select Borrow. Submit Compaction report to MMD for clearance.

4  per	1	Lane Mile per Lift

1  per	2000	Cubic Yard

# Aggregate Materials, Source Material

Plant or Product Qualification

| Evaluation of Production Facility for SATD Materials |  |  |  | Facility Qualification |
| --- | --- | --- | --- | --- |
| Qualification of Quarry | 1 | per | 1 | Prior to Source Request |
|  | 1 | per | 1 | Year |
| Review of Aggregate Quality |  |  |  | Product Qualification |
| Annual Quality of Coarse Aggregates | 1 | per | 1 | Prior to Source Request |
| 50 Lbs (or 35 Lbs for lightweight) in a Soils Bag | 1 | per | 1 | Year |
| Annual Quality of Fine Aggregates. | 1 | per | 1 | Prior to Source Request |
| 50 Lbs (40 lbs for lightweight) in a Soils Bag | 1 | per | 1 | Year |

# Asphalt Additives

## Plant or Product Qualification

Evaluation of Production Facility for ATD Materials	Facility Qualification

Production facility data maintained to track the material supply chain and provide a basis for qualified products.

1  per	1	Prior to Usage on Project

Evaluation of Material Product for ATD Materials	Product Qualification

Qualification of Material Product for use on State Projects	1  per	1	Prior to Usage on Project

# Asphalt Mixtures

## Plant or Product Qualification

| Evaluation of Production Facility for ATD Materials |  |  |  | Facility Qualification |
| --- | --- | --- | --- | --- |
| Production facility to be certified to produce material for State projects. | 1 | per | 12 | Months |
| Evaluation of Material Product for ATD Materials |  |  |  | Product Qualification |
| Review and Qualification of Asphalt Mixture Material Product. | 1 | per | 1 | Prior to Source Request |
| . |  |  |  |  |
| SHA Acceptance Facility Visit for Asphalt Mix Production |  |  |  | Product QC/QA |
| Production Quality Assurance | 1 | per | 6000 | Ton |
| . | 1 | per | 10 | Production Day |

SHA Acceptance of Binder Component	Product QC/QA

Asphalt Technology representative to witness and take possession of material sample.

1 Quart in a Friction Top Can

1  per	10	Production Day

1  per	1	Project Completion

1  per	6000	Ton

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing

.

1  per	1	Prior to Usage on Project

## Material Production

Notification of Production for ATD materials	Production Notification

Producer to notify the Asphalt Technology Division 1 day prior to production.

.

1  per	1	Placement Day

## Project Construction

| Core Sampling for Asphalt Mix Density Analysis |  |  |  | Material Sampling and Testing |
| --- | --- | --- | --- | --- |
| Project Engineer shall verify that the contractor takes QC and QA Density Cores at random locations in the pavement. (1 Sample = 5 Cores Min. See Material QA Manual for more information) | 2 | per | 1 | Production Day |
| 1 Sample = 5 - 6" Dia. Cores (min) |  |  |  |  |
| Density Gauge testing for Patches or Small Quantities |  |  |  | Material Sampling and Testing |
| Patch density measured at random locations with an asphalt density gauge, recorded on a Form 73-1P and submitted to OMT. See specification 505.03.14 for additional details. | 1 | per | 1 | Lift of each Patch |
| 2 Readings per test |  |  |  |  |
| Box Sampling for Asphalt Mixture |  |  |  | Material Sampling and Testing |
| Project Engineer shall verify that the contractor takes QC | 2 | per | 1000 | Ton |
| and QA Mix Box at random intervals during placement of asphalt mixture. | 2 | per | 1 | Production Day |
| 1 Sample = 1-50 LB Box (2-50 LB for 25.0mm Mix, 2-50 LB for 37.5mm Mix) |  |  |  |  |

Box Sampling for Patches or Small Daily Quantities of Asphalt Mixture	Material Sampling and Testing

Project Engineer shall verify that the contractor takes QC and QA Box Samples at random intervals at least once per mix for every 1000 tons or once per mix weekly, whichever yields the greater frequency. See 505.03.12 for additional details.

1 Sample = 1-50 LB Box (2-50 LB for 25.0mm Mix, 2-50 LB for 37.5mm Mix)

2  per	5	Placement Day

2  per	1000	Ton

Asphalt Mix Density Pay Factor Analysis	Sample Analysis

Density QA and QC results are to be processed by the Asphalt Technology Division to develop a recommended "Density Pay Factor".

1  per	1	Sample Set

Asphalt Mix Pay Factor Analysis	Sample Analysis

Mixture QA and QC results are to be processed by the Asphalt Technology Division to develop a recommended "Mixture Pay Factor".

1  per	1	Project Completion

1  per	6000	Ton

Evaluation of Pavement Surface Profile	Project Wide Testing

Surface profiling will be completed as indicated in Section 535 of the Special Provisions.

# Asphalt Release

1  per	1	Item Completion

## Plant or Product Qualification

Evaluation of Production Facility for ATD Materials	Facility Qualification

Production facility data maintained to provide a basis for qualified products.

1  per	1	Prior to Usage on Project

Evaluation of Material Product for ATD Materials	Product Qualification

Qualification of Material Product.	1  per	1	Prior to Usage on Project

# Cement Materials and Bagged Mixtures, Group 1

## Plant or Product Qualification

Evaluation of Production Facility for CTD Materials	Facility Qualification

Production facility data maintained to provide a basis for qualified products.

1  per	1	Prior to Source Request

Evaluation of Material Product for CTD Materials	Product Qualification

Qualification of Material Product for use on State Projects	1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

CTD Material Verification	Material Verification

Project Engineer to collect certifications (TC 1.03 w/o test data) and submit to OMT for clearance.

# Cement Materials and Bagged Mixtures, Group 2

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

CTD Material Review and Acceptance	Material Certification for Project Usage

Submit sample of material accompanied by a Form 88 and Material certification (1.03 w/o test data) to OMT for job specific approval.

1 Factory Sealed Container in a Factory Sealed Container

1  per	1	Prior to Usage on Project

## Project Construction

CTD Material Verification	Material Verification

Project Engineer to collect certifications (TC 1.03 w/o test data) and a material sample. Submit to OMT for verification and clearance

# Cement Materials and Bagged Mixtures, Group 3

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

CTD Material Review and Acceptance	Material Certification for Project Usage

Submit Form 88 and Material Certification (1.03 w/o test data) to OMT for job specific approval.

1  per	1	Prior to Usage on Project

## Project Construction

CTD Material Verification	Material Verification

Project Engineer to verify approval stamp.	1  per	1	Delivery to Project

# Cement Materials and Bagged Mixtures, Group 4

## Plant or Product Qualification

Evaluation of Production Facility for CTD Materials	Facility Qualification

Material Specific Qualification of Material Producer	1  per	1	Prior to Source Request

# Cement Treated Base/Cement Treated Subgrade

## Plant or Product Qualification

Evaluation of Production Facility for SATD Materials	Facility Qualification

Producer to perform daily gradations and moisture checks on aggregate materials.

1  per	1	8 Hour Shift

1  per	1000	Ton

Production Quality Assurance	1  per	10	Production Day

Quality Control Plan of Production Facility for state projects.

1  per	1	Prior to Source Request

## Source Approval

| Source Submission |  |  |  | Source of Supply Submittal |
| --- | --- | --- | --- | --- |
| Source of Supply Processing | 1 | per | 1 | Prior to Usage on Project |
| Mix Design | 1 | per | 1 | Material or Treatment Change |
|  | 1 | per | 1 | Prior to Usage on Project |

Material Production

SATD Material Review	Material Certification for Project Usage

Materials to be sampled at its place of origin. Project Engineer to contact SATD to schedule sampling.

1  per	1	Prior to Usage on Project

1  per	1	Prior to Usage on Project

Project Construction

| Project Site Testing |  |  |  | Material Sampling and Testing |
| --- | --- | --- | --- | --- |
| Construct a 500 foot long control strip onsite according to section 502.03.05 | 1 | per | 1 | Project |
| Acceptance of the control strip will be based on | 1 | per | 1 | Cement Modified Subgrade |
| performing Falling Weight Deflectometer (FWD) testing and analysis per Section 3.10 of the Pavement Performance Specifications and the Pavement and Geotechnical Design Guide | 1 | per | 1 | Cement Treated Base |
| Application Rate Verification by weight of cement | 1 | per | 1 | Truck Load |
| Project Engineer to submit FM 14 for Depth and Pulverization check | 3 | per | 1 | Placement Day |
| Compaction and Moisture analysis performed by Project | 1 | per | 1 | Placement Day |
| Engineer. Submit compaction report to MMD for clearance. | 2 | per | 2 | Lane Mile per Lift |

# Compost Materials

## Plant or Product Qualification

| Evaluation of Material Producer for LPD Materials |  | Facility Qualification |
| --- | --- | --- |
| Qualification of Compost Supplier for use on State projects | 1 per 1 | Prior to Source Request |
| Source Approval |  |  |
| Source Submission |  | Source of Supply Submittal |
| Source of Supply Processing | 1 per 1 | Prior to Usage on Project |

Project Construction

LPD Material Verification	Material Verification

Project Engineer to inspect compost certification provided by the Contractor with the delivery to verify that compost is of the correct type per 920.02.05, and that compost is sourced from a MDA or MDE approved producer. Project Engineer to visually inspect the placed material to ensure the compost is fit for usage and applied as specified.

Project Engineer to submit Form 14 with copy of product label or delivery ticket for clearance.

# Concrete Deck Protection

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

CTD Material Verification	Material Verification

Project Engineer to collect certifications (TC 1.03 w/o test data) and submit to OMT for clearance.

# Contract Specified Material Systems

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

LPD Material Verification	Material Verification

Project Engineer to collect manufacturers certification (TC 1.03 w/o test results) and fill out Form 14 indicating material was placed in accordance with documents.

Submit certification and Form 14 to OMT for clearance.

# Curing Compounds (Liquid Membrane)

1  per	1	Item Completion

## Plant or Product Qualification

Evaluation of Production Facility for CTD Materials	Facility Qualification

Production facility data maintained to provide a basis for qualified products.

1  per	1	Prior to Usage on Project

Evaluation of Material Product for CTD Materials	Product Qualification

Qualification of Material Product for use on State Projects.	1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

CTD Material Verification	Material Verification

Project Engineer to collect certifications (TC 1.03 w/ test data) and submit to OMT for clearance.

# Decorative Concrete Finish, Horizontal Surface

1  per	1	Delivery to Project

## Plant or Product Qualification

Evaluation of Production Facility for CTD Materials	Facility Qualification

Material Specific Qualification of Material Producer	1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

CTD Material Verification	Material Verification

Project Engineer to inspect placed materials and submit Form 14 to MMD for clearance.

# Decorative Concrete Stains, Vertical Surface

1  per	1	Item Completion

## Plant or Product Qualification

Evaluation of Production Facility for CTD Materials	Facility Qualification

Production facility data maintained to provide a basis for qualified products.

1  per	1	Prior to Source Request

Evaluation of Material Product for CTD Materials	Product Qualification

Qualification of Material Product for use on State Projects.	1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

CTD Material Verification	Material Verification

Project Engineer to collect manufacturer’s material certifications (TC 1.03 w/ test data) and submit to MMD for clearance.

# Decorative Reinforced Thermoplastic

1  per	1	Delivery to Project

## Plant or Product Qualification

Evaluation of Material Producer for LPD Materials	Product Qualification

Product Qualification	1  per	5	Year

## Source Approval

Source Submission	Source of Supply Submittal

Sources of Supply Processing	1  per	1	Prior to Source Approval

## Project Construction

LPD Material Verification	Material Verification

Material/Product Verification at Project Site. Project Engineer to verify material product, and submit Form 14 for material clearance, which validates the following: Verifying that the imprinting tools and materials are compatible; Monitoring the Contractor/subcontractor conformance with the Quality Control Plan; Verifying the Contractor/subcontractor qualifications to produce this type of markings and comply with these and the

manufacturer’s specifications; Verifying the actual results of all Quality Control tests for the actual materials in the batch submitted for the project.

1  per	1	Item Completion

1  per	1	Prior to Usage on Project

# Electrical Accessories

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

Approval of Material Prior to Shipment	Material Certification for Project Usage

Producer to submit Catalog Cuts to the Office of Traffic and Safety.

1  per	1	Prior to Usage on Project

## Project Construction

OOTS Material Verification	Material Verification

Project Engineer to verify material product, submit Form 14.

# Emulsified Asphalts, Other

1  per	1	Delivery to Project

## Plant or Product Qualification

Evaluation of Production Facility for ATD Materials	Facility Qualification

Production facility to be certified to produce material for State projects.

1  per	12	Months

Evaluation of Material Product for ATD Materials	Product Qualification

Qualification of Material Product for use on State Projects.	1  per	1	Prior to Usage on Project

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

ATD Material Verification	Material Verification

Project Engineer to collect certifications (TC 1.03 w/ test data), FORM 88, and material samples. Submit items to OMT for testing and clearance.

1 Gallon in a Widemouth Plastic Jar

# Emulsified Asphalts, Tack Coat

1  per	1	Item Completion

## Plant or Product Qualification

Evaluation of Production Facility for ATD Materials	Facility Qualification

Production facility to be certified to produce material for State projects.

1  per	12	Months

Evaluation of Material Product for ATD Materials	Product Qualification

Qualification of Material Product for use on State Projects	1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

ATD Material Verification	Material Verification

Project Engineer to collect certifications (TC 1.03 w/ test data), FORM 88, and material samples. Submit items to OMT for testing and clearance.

1 Gallon in a Widemouth Plastic Jar

# Fertilizers

1  per	1	Item Completion

## Plant or Product Qualification

Evaluation of Material Producer for LPD Materials	Facility Qualification

Qualification of Fertilizer producer for use on State projects

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

LPD Material Verification	Material Verification

Project Engineer to verify that fertilizer is from the correct source. Project Engineer to inspect fertilizer labels, visually inspect fertilizer, and verify fertilizer composition and proposed application rates. Project Engineer to verify fertilizer usage and submit Form 14 with fertilizer labels for material clearance.

# Foamed Asphalt Stabilized Base Course

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

# Form Release

## Plant or Product Qualification

Evaluation of Production Facility for CTD Materials	Facility Qualification

Production facility data maintained to provide a basis for qualified products.

1  per	1	Prior to Source Request

Evaluation of Material Product for CTD Materials	Product Qualification

Qualification of Material Product for use on State Projects.	1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

CTD Material Verification	Material Verification

Project Engineer to inspect placed material and submit Form 14.

# Geosynthetic Materials, Geotextiles

1  per	1	Delivery to Project

## Plant or Product Qualification

Evaluation of Production Facility for SATD Materials	Facility Qualification

Cursory Plant data record review, required for qualified products.

1  per	1	Prior to Source Request

Evaluation of Material Product for SATD Materials	Product Qualification

| Qualification of Material Product. | 1 | per | 1 | Prior to Source Request |
| --- | --- | --- | --- | --- |
|  | 1 | per | 24 | Months |

Material Product QA for SATD Materials	Product QC/QA

Quality Assurance of Delivered Products	1  per	3	Months

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

Material Verification for SATD Materials	Material Verification

Project Engineer to receive certified roll data (TC1.03 w/ test data) and submit to MMD for clearance.

# Geosynthetic Materials, Other

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

Material Verification for SATD Materials	Material Verification

Project Engineer to verify material.	1  per	1	Delivery to Project

# Latex Emulsion

## Plant or Product Qualification

Evaluation of Production Facility for CTD Materials	Facility Qualification

Production facility data maintained to provide a basis for qualified products.

1  per	1	Prior to Usage on Project

Evaluation of Material Product for CTD Materials	Product Qualification

Qualification of Material Product for use on State Projects.	1  per	1	Prior to Usage on Project

# Liquid Pavement Marking

## Plant or Product Qualification

Pavement Marking Facility Review	Facility Qualification

Inspection of Production Facility	1  per	36	Months

Pavement Marking Product Review	Product Qualification

Qualification of Material Product	1  per	1	Prior to Source Request

Pavement Marking Product Acceptance	Product QC/QA

Material sample to be taken by SHA and Producer to provide material certification conforming to TC 1.03 w/ test data to SHA for review, testing, and stamping. The stamped certification will be returned to the producer.

.

1  per	1	Batch, Lot or Heat

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

Pavement Marking Material Verification at Project Site	Material Verification

Project Engineer to collect manufacture’s certifications (TC 1.03 w/ test data) and OMT stamped documentation approving the material batch, submit to MMD for clearance.

1  per	1	Delivery to Project

Post Placement Project Wide Testing	Project Wide Testing

Field Testing at Project Site by the Pavement Marking Team as per MSMT 729.

# Miscellaneous Chemical Materials

1  per	1	Item Completion

## Project Construction

CTD Material Verification	Material Verification

Project Engineer to collect certifications (TC 1.03 w/ test data) and submit certs and Form 14 to OMT for clearance.

# Miscellaneous Landscape Materials

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

Visual Inspection of Placed Material	Material Sampling and Testing

Project Engineer to inspect material. Project Engineer to submit Form 14 for material clearance.

# Miscellaneous Materials

1  per	1	Delivery to Project

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing.	1  per	1	Prior to Usage on Project

## Project Construction

LPD Material Verification	Material Verification

Project Engineer to inspect placed material and submit Form 14.

Project Engineer to collect certifications (TC 1.03 w/ test data) and submit certs to OMT for clearance.

# Miscellaneous Materials with Certifications

1  per	1	Delivery to Project

1  per	1	Delivery to Project

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

LPD Material Verification	Material Verification

Project Engineer to collect material certifications (TC 1.03 w/o test data) and submit to OMT for clearance.

# Mulch

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

Visual Inspection of Placed Material	Material Sampling and Testing

Project Engineer to inspect placed material to verify that it from the approved source and fit for use. Project Engineer to verify that mulch is placed uniformly and correctly during and after placement. Project Engineer to submit Form 14 for material clearance.

# Pavement Markers

1  per	1	Delivery to Project

## Plant or Product Qualification

Pavement Marking Facility Review	Facility Qualification

Inspection of Production Facility	1  per	24	Months

Pavement Marking Product Review	Product Qualification

Qualification of Material Product	1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

Pavement Marking Material Verification at Project Site	Material Verification

Project Engineer to collect manufacturer's Certification (TC 1.03 w/o test data), and submit certifications to MMD for clearance.

1  per	1	Delivery to Project

Post Placement Project Wide Testing	Project Wide Testing

Field Testing at Project Site by the Pavement Marking Team as per MSMT 729.

# Pavement Marking Mat'l: Other

1  per	1	Item Completion

## Plant or Product Qualification

Pavement Marking Facility Review	Facility Qualification

Inspection of Production Facility	1  per	12	Months

Pavement Marking Product Review	Product Qualification

Evaluate new material products through the MPEL process	1  per	1	Prior to Usage on Project

Pavement Marking Product Acceptance	Product QC/QA

Producer to submit material certification conforming to TC

1.03 w/ test data to OMT's Pavement Marking team for review, stamping, and return.

1  per	1	Batch, Lot or Heat

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

Pavement Marking Material Verification at Project Site	Material Verification

Project Engineer to collect OMT stamped manufacturer's certification (TC 1.03 w/ test data) and submit them to MMD for clearance.

# Pavement Marking Preformed Thermoplastic

1  per	1	Delivery to Project

## Plant or Product Qualification

Pavement Marking Facility Review	Facility Qualification

Inspection of Production Facility	1  per	24	Months

Pavement Marking Product Review	Product Qualification

Qualification of Material Product	1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

Pavement Marking Material Verification at Project Site	Material Verification

Project Engineer to collect manufacturer's Certification (TC 1.03 w/o test data), and submit certifications to MMD for clearance.

1  per	1	Delivery to Project

Post Placement Project Wide Testing	Project Wide Testing

Field Testing at Project Site by the Pavement Marking Team as per MSMT 729.

# Pavement Marking Tape

1  per	1	Item Completion

## Plant or Product Qualification

| Pavement Marking Facility Review Inspection of Production Facility | 1 | per | 24 | Months | Facility Qualification |
| --- | --- | --- | --- | --- | --- |
| Pavement Marking Product Review Qualification of Material Product | 1 | per | 1 | Prior to Source | Product Qualification Request |

Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

Pavement Marking Material Verification at Project Site	Material Verification

Project Engineer to collect manufacturer's Certification (TC 1.03 w/o test data), and submit certifications to MMD for clearance.

1  per	1	Delivery to Project

Post Placement Project Wide Testing	Project Wide Testing

Field Testing at Project Site by the Pavement Marking Team as per MSMT 729.

# Pavement Repair Materials

1  per	1	Item Completion

## Plant or Product Qualification

Review of Producer (QPL)	Facility Qualification

Production facility data maintained to provide basis for qualified products.

1  per	1	Prior to Source Request

Review of Product (QPL)	Product Qualification

Qualification of Material Product for use on State Projects.	1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

ATD Material Verification	Material Verification

Project Engineer to collect certifications (TC 1.03 w/o test data) and submit certs to OMT for clearance.

# Performance Graded Asphalt Binder

1  per	1	Delivery to Project

## Plant or Product Qualification

Evaluation of Production Facility for ATD Materials	Facility Qualification

Qualification of Binder Supplier for use on State projects	1  per	1	Prior to Usage on Project

Evaluation of Material Product for ATD Materials	Product Qualification

Qualification of Material Product.	1  per	1	Batch, Lot or Heat

# Plant Materials

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

LPD Material Review	Material Certification for Project Usage

LPD to inspect plant materials before installation. LPD to inspect plant materials after installation. LPD to submit Form 14 for materials clearance.

# Portland Cement Concrete Mixtures

1  per	1	Prior to Usage on Project

## Plant or Product Qualification

| Evaluation of Production Facility for CTD Materials |  |  |  | Facility Qualification |
| --- | --- | --- | --- | --- |
| Production facility to be certified to produce material for | 1 | per | 1 | Prior to Source Request |
| State projects. | 1 | per | 12 | Months |
| SHA Acceptance Facility Visit for CTD Material Production |  |  |  | Facility Qualification |
| OMT Personnel to perform Quality Assurance on concrete production processes. | 1 | per | 10 | Production Day |
| 75 Lbs in a Soils Bag |  |  |  |  |
| Evaluation of Material Product for CTD Materials |  |  |  | Product Qualification |
| Review and Qualification of Portland Cement Concrete Mixture Material Product. | 1 | per | 1 | Prior to Source Request |
| Material Product QC |  |  |  | Product Qualification |
| Producer to perform daily gradations and moisture tests on aggregate materials. | 2 | per | 1 | Production Day |
| 10 LBS - Fine Agg, 35 LBS Lt. wt., 50 LBS Coarse. in a Soils Bag |  |  |  |  |

Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

Notification of Production for CTD materials	Production Notification

Producer to notify OMT one working day prior to production at concrete@sha.state.md.us

1  per	1	Production Day

Project Construction

| CTD Material Verification |  |  |  | Material Verification |
| --- | --- | --- | --- | --- |
| Project Engineer to conduct field tests. (Air Entrainment, Slump, etc.). | 1 | per | 1 | Delivery to Project |
| Project Engineer to collect certifications (TC 1.03 w/ test data) and submit to OMT for clearance. | 1 | per | 1 | Delivery to Project |
| Concrete Sampling and Testing |  |  |  | Material Sampling and Testing |
| Project Engineer to mold acceptance cylinders, Prime | 1 | per | 50 | Cubic Yard |
| Contractor to cure and transport cylinders to OMT for testing. | 1 | per | 1 | Production Day |
| 2 Cylinders = 1 Sample |  |  |  |  |
| Mix 7 -Project Engineer to mold acceptance cylinders, Prime Contractor to cure and transport cylinders to OMT for testing. | 3 | per | 1 | Placement Day |
| 2 Cylinders = 1 Sample |  |  |  |  |
| Pay Factor Calculation |  |  |  | Sample Analysis |
| OMT to perform statistical analysis on all acceptance concrete cylinder tests for project. | 1 | per | 1 | Item Completion |

# Portland Cement Concrete Mixtures, Latex Modified

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

.

1  per	1	Prior to Source Request

Evaluation of Production Facility for CTD Materials	Facility Qualification

Detailed Qualification of Production Facility.	1  per	1	Prior to Usage on Project

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing

.

1  per	1	Prior to Usage on Project

## Project Construction

CTD Material Verification	Material Verification

Project Engineer to perform concrete plastic tests.

Typically one slump and one air entrainment.

1  per	1	Delivery to Project

Chemical Tests	Material Sampling and Testing

Submit a sample or certification (TC 1.03 w/ test data) of each component to OMT for verification.

2 Quarts - Latex, 1 Quart Each Admixture in a Plastic Jug

1  per	1	Lot / Production Day

Concrete Sampling and Testing	Material Sampling and Testing

Submit sample to OMT for testing.	2  per	1	Truck

Pay Factor Calculation	Sample Analysis

OMT to perform statistical analysis on all acceptance concrete cylinder tests for project.

# Precast Concrete, Drainage Structures

1  per	1	Item Completion

## Plant or Product Qualification

Evaluation of Production Facility for CTD Materials	Facility Qualification

Facility to be qualified (and re-qualified annually) for state projects before it is sourced to a project.

1  per	12	Months

Quality Control for Aggregate Material Gradation	Facility QA/QC

Producer to perform gradation quality control as per AASHTO T27.

17 lbs for coarse; 500 grams for fine

1  per	7	Production Day

### SHA Acceptance Review for Aggregate Material Gradation.	Facility QA/QC

Concrete Technology representative to witness gradation quality control process of producer.

.

1  per	30	Production Day

Quality Control for Aggregate Moisture Content	Facility QA/QC

Producer to perform moisture quality control as per MSMT 251.

17 lbs for coarse; 500 grams for fine

1  per	1	Production Day

SHA Acceptance Review of Aggregate Moisture Content	Facility QA/QC

Concrete Technology representative to witness moisture quality control

.

1  per	30	Production Day

SHA Acceptance Review for Steel Reinforcing	Facility QA/QC

Deformed Steel bars to be sampled by producer. A Concrete Technology representative will witness the sampling, fill out Form 88, and deliver sample to the OMT laboratory.

3 - 2 foot lengths

1  per	90	Production Day

SHA Acceptance Review for Admixture Materials	Facility QA/QC

Producer to sample all admixture materials and provide to Concrete Technology for evaluation.

1 Quart in a Screw Top Can

1  per	30	Production Day

SHA Acceptance Review for Cementitious Materials.	Facility QA/QC

Producer to sample all cementitious materials and provide to Concrete Technology for evaluation, as per 902.03.

10 lbs in a Plastic Jug

1  per	3	Months

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

Notification of Production for CTD materials	Production Notification

Producer to notify the Concrete Technology Division prior to production at concrete@sha.state.md.us. Please provide the design standard with the notification.

1  per	1	Prior to Usage on Project

CTD Material Review and Acceptance	Material Certification for Project Usage

Submit copies of any shop drawings, specifications, or plan sheets to the designer as per the Invitation for Bids document.

1  per	1	Prior to Usage on Project

## Project Construction

CTD Material Verification	Material Verification

Project Engineer to visually inspect precast elements, record all QC stamps on a Form 14, and verify stamp matches the certification. Collect manufacture's certification and submit it along with the Form 14 to MMD for clearance.

# Precast Concrete, Miscellaneous

1  per	1	Delivery to Project

## Plant or Product Qualification

Evaluation of Production Facility for CTD Materials	Facility Qualification

Facility to be qualified (and re-qualified annually) for state projects before it is sourced to a project.

1  per	3	Year

Quality Control for Aggregate Material Gradation	Facility QA/QC

Producer to perform gradation quality control as per AASHTO T27

17 lbs for coarse; 500 grams for fine

1  per	7	Production Day

### SHA Acceptance Review for Aggregate Material Gradation.	Facility QA/QC

Concrete Technology representative to witness gradation quality control process of producer.

.

1  per	2	Year

Quality Control for Aggregate Moisture Content	Facility QA/QC

Producer to perform moisture quality control as per MSMT 251.

17 lbs for coarse; 500 grams for fine

1  per	1	Production Day

SHA Acceptance Review of Aggregate Moisture Content	Facility QA/QC

Concrete Technology representative to witness moisture quality control

.

1  per	2	Year

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

Notification of Production for CTD materials	Production Notification

Producer to notify the Concrete Technology Division between 48 hours prior to shipment and end of shipping day at concrete@sha.state.md.us.

1  per	1	Prior to Usage on Project

## Project Construction

CTD Material Verification	Material Verification

Project Engineer to visually inspect precast elements, record all QC stamps on a Form 14, and verify stamp matches the certification. Collect manufacture's Certification and submit it along with the Form 14 to MMD for clearance.

# Precast Concrete, Pipe

1  per	1	Delivery to Project

## Plant or Product Qualification

| Evaluation of Production Facility for CTD Materials |  |  |  | Facility Qualification |
| --- | --- | --- | --- | --- |
| Facility to be qualified (and re-qualified annually) for state | 1 | per | 1 | Prior to Source Request |
| projects before it is sourced to a project. | 1 | per | 12 | Months |
| . |  |  |  |  |
| SHA Acceptance Facility Visit for CTD Material Production |  |  |  | Facility Qualification |
| Quality Assurance of Pipe Production | 1 | per | 1000 | Each |
| . | 1 | per | 30 | Production Day |

Quality Control for Aggregate Material Gradation	Facility QA/QC

Producer to perform gradation quality control as per AASHTO T27

17 lbs for coarse; 500 grams for fine

1  per	7	Production Day

### SHA Acceptance Review for Aggregate Material Gradation.	Facility QA/QC

Concrete Technology representative to witness gradation quality control process of producer.

.

1  per	30	Production Day

Quality Control for Aggregate Moisture Content	Facility QA/QC

Producer to perform moisture quality control as per MSMT 251.

17 lbs for coarse; 500 grams for fine

1  per	1	Production Day

SHA Acceptance Review of Aggregate Moisture Content	Facility QA/QC

Concrete Technology representative to witness moisture quality control

.

1  per	30	Production Day

SHA Acceptance Review for Admixture Materials	Facility QA/QC

Producer to sample all admixture materials and provide to Concrete Technology for evaluation.

1 Quart in a Screw Top Can

1  per	30	Production Day

SHA Acceptance Review for Cementitious Materials.	Facility QA/QC

Producer to sample all cementitious materials and provide to Concrete Technology for evaluation, as per 902.03.

10 lbs in a Plastic Jug

1  per	1	Months

1  per	10	Production Day

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

Notification of Production for CTD materials	Production Notification

Producer to notify the Concrete Technology Division between 48 hours prior to shipment and end of shipping day at concrete@sha.state.md.us.

1  per	1	Prior to Usage on Project

CTD Material Review and Acceptance	Material Certification for Project Usage

Plant QC Personnel to perform lot inspection	1  per	1	Prior to Usage on Project

## Project Construction

CTD Material Verification	Material Verification

Project Engineer to visually inspect pipe, record all QC Stamps from pipe on a Form 14, and verify a pipe stamp matches the certification. Collect manufacture’s Certification and submit it along with the Form 14 to MMD for Clearance.

# Precast Concrete, Prestressed and Structural

1  per	1	Delivery to Project

## Plant or Product Qualification

Evaluation of Production Facility for CTD Materials	Facility Qualification

Facility to be qualified (and re-qualified annually) for state projects before it is sourced to a project.

.

1  per	12	Months

Quality Control for Aggregate Material Gradation	Facility QA/QC

Producer to perform gradation quality control as per AASHTO T27.

17 lbs for coarse; 500 grams for fine

1  per	7	Production Day

### SHA Acceptance Review for Aggregate Material Gradation.	Facility QA/QC

Concrete Technology representative to witness gradation quality control process of producer.

.

1  per	30	Production Day

Quality Control for Aggregate Moisture Content	Facility QA/QC

Producer to perform moisture quality control as per MSMT 251.

17 lbs for coarse; 500 grams for fine

1  per	1	Production Day

SHA Acceptance Review of Aggregate Moisture Content	Facility QA/QC

Concrete Technology representative to witness moisture quality control

.

1  per	30	Production Day

SHA Acceptance Review for Steel Reinforcing	Facility QA/QC

Deformed Steel bars to be sampled by producer. A Concrete Technology representative will witness the sampling, fill out Form 88 and deliver sample to the OMT laboratory.

3 - 2 foot lengths

1  per	90	Production Day

SHA Acceptance Review for Admixture Materials	Facility QA/QC

Producer to sample all admixture materials and provide to Concrete Technology for evaluation.

1 Quart in a Screw Top Can

1  per	30	Production Day

SHA Acceptance Review for Cementitious Materials.	Facility QA/QC

Producer to sample all cementitious materials and provide to Concrete Technology for evaluation.

1  per	1	Months

1  per	10	Production Day

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

Notification of Production for CTD materials	Production Notification

Producer to submit Shop Drawings and provide Production Notice to the Concrete Technology Division (concrete@sha.state.md.us) 30 business days before commencing production of any prestressed or other structural concrete items.

1  per	1	Prior to Usage on Project

CTD Material Review and Acceptance	Material Certification for Project Usage

Direct Inspection at Facility during Casting, Approval of Material for Project Use.

1  per	1	Prior to Usage on Project

## Project Construction

CTD Material Verification	Material Verification

Project Engineer to visually inspect precast elements, record all stamps on a Form 14, and verify stamps match the certification. Collect manufacture's certification and submit it along with the Form 14 to MMD for clearance.

# Precast Concrete, Walls

1  per	1	Delivery to Project

## Plant or Product Qualification

| Evaluation of Production Facility for CTD Materials |  |  |  | Facility Qualification |
| --- | --- | --- | --- | --- |
| Facility to be qualified (and re-qualified annually) for state | 1 | per | 1 | Prior to Usage on Project |
| projects before it is sourced to a project. | 1 | per | 12 | Months |
| . |  |  |  |  |
| Quality Control for Aggregate Material Gradation |  |  |  | Facility QA/QC |
| Producer to perform gradation quality control as per AASHTO T27 | 1 | per | 7 | Production Day |
| 17 lbs for coarse; 500 grams for fine |  |  |  |  |
| SHA Acceptance Review for Aggregate Material Gradation. |  |  |  | Facility QA/QC |
| Concrete Technology representative to witness gradation quality control process of producer. | 1 | per | 30 | Production Day |
| . |  |  |  |  |
| Quality Control for Aggregate Moisture Content |  |  |  | Facility QA/QC |
| Producer to perform moisture quality control as per MSMT 251. | 1 | per | 1 | Production Day |
| 17 lbs for coarse; 500 grams for fine |  |  |  |  |
| SHA Acceptance Review of Aggregate Moisture Content |  |  |  | Facility QA/QC |
| Concrete Technology representative to witness moisture quality control | 1 | per | 30 | Production Day |
| . |  |  |  |  |
| SHA Acceptance Review for Admixture Materials |  |  |  | Facility QA/QC |
| Producer to sample all admixture materials and provide to Concrete Technology for evaluation. | 1 | per | 30 | Production Day |
| 1 Quart in a Screw Top Can |  |  |  |  |
| SHA Acceptance Review for Cementitious Materials. |  |  |  | Facility QA/QC |

Producer to sample all cementitious materials and provide to Concrete Technology for evaluation.

10 lbs in a Plastic Jug

1  per	1	Months

1  per	10	Production Day

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

Notification of Production for CTD materials	Production Notification

Producer to submit Shop Drawings and provide Production Notice to the Concrete Technology Division (concrete@sha.state.md.us) 30 business days before commencing production of any precast MSE or Noise Barrier components.

1  per	1	Prior to Usage on Project

CTD Material Review and Acceptance	Material Certification for Project Usage

Direct Inspection at Facility during Casting, Approval of Material for Project Use.

1  per	1	Prior to Usage on Project

Test Panel Verification	Material Certification for Project Usage

Test panel to be evaluated by OMT, LOD and OOS.	1  per	1	Prior to Usage on Project

## Project Construction

CTD Material Verification	Material Verification

Project Engineer to visually inspect precast elements, record all stamps on a Form 14, and verify stamps match the certification. Collect manufacture's certification and submit it along with the Form 14 to MMD for clearance.

# Recycled Materials for HMA Mixtures

1  per	1	Delivery to Project

## Plant or Product Qualification

| Evaluation of Production Facility for ATD Materials |  |  | Facility Qualification |
| --- | --- | --- | --- |
| Joint Qualification with Asphalt Mix production facility. | 1 per | 1 | Prior to Source Request |
| Evaluation of Material Product for ATD Materials |  |  | Product Qualification |
| Qualification of Material Product. | 1 per | 1 | Prior to Source Request |
| Source Approval |  |  |  |
| Source Submission |  |  | Source of Supply Submittal |
| Source of Supply Processing | 1 per 1 |  | Prior to Usage on Project |

Project Construction

ATD Material Verification	Material Verification

Project Engineer to visually inspect placed material and submit Form 14 to OMT for clearance.

# Reflective Sheeting

1  per	1	Item Completion

## Plant or Product Qualification

Review Producer (OOTS)	Facility Qualification

Qualification of Production Facility	1  per	1	Prior to Source Request

SM Production QA	Facility Qualification

| Production Quality Assurance. | 1 | per | 1 | Prior to Usage on Project |
| --- | --- | --- | --- | --- |
|  | 1 | per | 12 | Months |

Review Product (OOTS)	Product Qualification

Qualification of Material Product	1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

OOTS Material Verification	Material Verification

See source response for "Aluminum Signs" for this item for acceptance

# Sealers: Qualified Liquid Materials

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Producer (QPL)	Facility Qualification

Production facility data maintained to provide a basis for qualified products.

1  per	1	Prior to Source Request

Review of Product (QPL)	Product Qualification

Qualification of Material Product for use on State Projects.	1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

LPD Material Verification	Material Verification

Project Engineer to collect certifications (TC1.03 w/ test data) and submit certifications to OMT for clearance.

# Seed for Mixes

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

LPD Material Verification	Material Verification

Project Engineer to inspect labels, seed material, seed mixtures, and seed application methods. Project Engineer to submit copies of labels with Form 14 for material clearance.

# SM Group 1 - General Approval

1  per	1	Item Completion

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

Material Verification at Project Site, Structural Materials	Material Verification

Project Engineer to submit Form 14 to the Materials Management Division confirming the material and its placement are acceptable and conform to specifications.

# SM Group 2 - General Approval with Certification

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

Material Verification at Project Site, Structural Materials	Material Verification

Project Engineer to collect manufacturer's certification (TC 1.03 w/o test data) indicating the specification to which the material conforms. Submit certification with Form 14 Stamp to the Materials Management Division for clearance. Submit the Domestic Materials Self-Certification Form to Materials Management Division for materials clearance.

Project Engineer to collect manufacturer's certification (TC 1.03 with test data) indicating the specification to which the material conforms. Submit certification with Form 14 Stamp to the Materials Management Division for clearance. Submit the Domestic Materials Self-Certification Form to Materials Management Division for materials clearance.

# SM Group 3 - Evaluation Before Shipment

1  per	1	Delivery to Project

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

OMT approval of material for shipment, Structural Materials	Material Certification for Project Usage

Submit Material Certification (TC 1.03 w/ Batch Specific Test Data) to metals@mdot.maryland.gov for review prior to delivery. If acceptable the document will be stamped by OMT and returned to the supplier to accompany the material to the project site.

The Structural Materials team or an Authorized Representative will inspect the material, all relevant certifications, and may take material samples at the production facility. Please contact metals@mdot.maryland.gov to schedule an inspection.

Submit Material Certification (TC 1.03 w/o test data) for timber preservatives to metals@mdot.maryland.gov. If acceptable the document will be stamped by OMT and returned to the source of supply to accompany the material to the project site.

Submit Sample, Form 88 and Material Certification (TC 1.03 w/o test data) for clay brick materials to OMT for evaluation. Form 88 will be returned to PE. Alternate sampling may be requested by contacting metals@mdot.maryland.gov 3 weeks prior to delivery.

10 Bricks

Submit Sample, Form 88 and Material Certification (TC 1.03 w/o test data) for concrete block to OMT for evaluation. Form 88 will be returned to PE. Alternate sampling may be requested by contacting metals@mdot.maryland.gov 3 weeks prior to delivery.

6 Blocks

1  per	1	Prior to Usage on Project

1  per	1	Prior to Usage on Project

1  per	1	Prior to Usage on Project

1  per	50000	Each

1  per	6000	Each

## Project Construction

Material Verification at Project Site, Structural Materials	Material Verification

Project Engineer to collect OMT stamped documentation indicating review and approval of material. Submit document to the Materials Management Division for materials clearance. Submit the Domestic Materials Self-Certification Form to Materials Management Division for materials clearance.

# SM Group 4 - Detectable Warning Surfaces

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Producer (SM)	Facility Qualification

Production facility data maintained to track the material supply chain and provide a basis for qualified products.

1  per	1	Prior to Source Request

| Review of Product (SM): |  | Product Qualification |
| --- | --- | --- |
| Qualification of Material Product for use on State Projects. | 1 per 1 | Prior to Source Request |
| Source Approval |  |  |
| Source Submission |  | Source of Supply Submittal |
| Source of Supply Processing | 1 per 1 | Prior to Usage on Project |

## Project Construction

Material Verification at Project Site, Structural Materials	Material Verification

Project Engineer to collect certifications (TC 1.03 w/o test data) and submit certs to OMT for clearance. Submit the Domestic Materials Self-Certification Form to Materials Management Division for materials clearance.

# SM Group 5 - Producer and Batch Data Tracked

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

Review of Product (SM):	Product Qualification

Maintain data on each heat or batch of product used on State projects.

1  per	1	Batch, Lot or Heat

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

OMT approval of material for shipment, Structural Materials	Material Certification for Project Usage

Batch/Heat of Material must be approved by OMT. The producer to submit Material Certification (TC 1.03 w/ test data) and Sample to Structural Materials for evaluation. Contact metals@mdot.maryland.gov for further information.

1  per	1	Batch, Lot or Heat

## Project Construction

Material Verification at Project Site, Structural Materials	Material Verification

Project Engineer to collect OMT stamped Material Certification (TC 1.03 w/ test data) and submit to the Materials Management Division for materials clearance. Submit the Domestic Materials Self-Certification Form to Materials Management Division for materials clearance.

# SM Group 6 - Qualified Facilities, Limited Review

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Producer (SM)	Facility Qualification

Facility to be qualified for state projects (and re-qualified annually) and issued an OMT certification stamp before it is sourced to a project. Submit the Domestic Materials Self-Certification Form to Materials Management Division for materials clearance.

1  per	1	Prior to Source Request

1  per	12	Months

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

Quality Assurance of Structural Material production facilities.	Material Certification for Project Usage

Facility re-qualification required, Structural Materials or an Authorized Representative to conduct facility evaluation and reissue facility certification. Please contact metals@mdot.maryland.gov to schedule an evaluation.

1  per	12	Months

## Project Construction

Material Verification at Project Site, Structural Materials	Material Verification

Project Engineer to collect the stamped supplier's Certification of Compliance listing the materials shipped and submit to the Materials Management Division for materials clearance.

# SM Group 7 - Qualified Facilities, Cert Review

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Producer (SM)	Facility Qualification

Facility to be qualified for state projects before it is sourced.

1  per	12	Months

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

Quality Assurance of Structural Material production facilities.	Material Certification for Project Usage

Facility re-qualification required. Structural Materials or an Authorized Representative to conduct facility evaluation prior to material approval. Contact metals@mdot.maryland.gov to determine inspection schedule.

1  per	12	Months

OMT approval of material for shipment, Structural Materials	Material Certification for Project Usage

Submit Material Certification (TC 1.03 w/batch test data). All Material Test Result (MTR’s) for steel and iron products must include a statement that material was produced (Melted and Manufactured in the United States) and sent to metals@mdot.maryland.gov for review and approval. If acceptable, the documents will be stamped and returned to the vendor to accompany the delivery.

1  per	1	Prior to Usage on Project

Submit Material Certification (TC 1.03 w/ test data) and a sample to Structural Materials, contact metals@mdot.maryland.gov. If acceptable the document will be stamped by OMT and returned to the source of supply to accompany the delivery.

1  per	1	Prior to Usage on Project

## Project Construction

Material Verification at Project Site, Structural Materials	Material Verification

Project Engineer to collect OMT stamped documentation indicating review and approval of material. Submit document to the Materials Management Division for materials clearance. Submit the Domestic Materials Self-Certification Form to Materials Management Division for materials clearance.

# SM Group 8 - Qualified Facilities, Production Insp

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Producer (SM)	Facility Qualification

Facility to be qualified for state projects before it is sourced.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

Quality Assurance of Structural Material production facilities.	Material Certification for Project Usage

Facility re-qualification required. Structural Materials to conduct facility evaluation and reissue facility certification.

1  per	12	Months

OMT approval of material for shipment, Structural Materials	Material Certification for Project Usage

The Metals team or an Authorized Representative will inspect the fabrication, all relevant certifications, and may take material samples at the production facility. Please contact metals@mdot.maryland.gov to determine inspection schedule.

1  per	1	Prior to Usage on Project

## Project Construction

Material Verification at Project Site, Structural Materials	Material Verification

Project Engineer to collect OMT stamped documentation indicating review and approval of material. Submit document to the Materials Management Division for materials clearance. Submit the Domestic Materials Self-Certification Form to Materials Management Division for materials clearance. Submit the Domestic Materials Self-Certification Form to Materials Management Division for materials clearance.

# SM Group 9 - Qualified Facilities, Not Sourced

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Producer (SM)	Facility Qualification

Facility to be qualified for state projects (and re-qualified annually).

# Sod & Seed Mixes with MDA Labels

1  per	12	Months

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

LPD Material Verification	Material Verification

Project Engineer to inspect and verify labels or tickets. Project Engineer to submit copy of label or ticket with Form 14 for material clearance.

# Soil Amendments

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

LPD Material Verification	Material Verification

Project Engineer to inspect labels and verify composition of material product. Project Engineer to determine that material is fit for use and applied as specified. Project Engineer to submit copy of product label with Form 14 for material clearance.

# Soil Materials, Fill Soil

1  per	1	Item Completion

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

SATD Material Review	Material Certification for Project Usage

Material to be sampled as Common Borrow at its place of origin. Project Engineer to contact SATD to schedule a sampling.

35 LBS in a Soils Bag

2  per	1	Prior to Usage on Project

Material to be sampled as Capping Borrow at its place of origin. Project Engineer to contact SATD to schedule a sampling.

35 LBS in a Soils Bag

Material to be sampled as Modified Borrow at its place of origin. Project Engineer to contact SATD to schedule a sampling.

35 LBS in a Soils Bag

Material to be sampled as Select Borrow at its place of origin. Project Engineer to contact SATD to schedule a sampling.

35 LBS in a Soils Bag

Material to be sampled as Clay Core material at its place of origin. Project Engineer to contact SATD to schedule a sampling

35 LBS in a Soils Bag

2  per	1	Prior to Usage on Project

2  per	1	Prior to Usage on Project

2  per	1	Prior to Usage on Project

2  per	1	Prior to Usage on Project

## Project Construction

| Project Sampling and Lab Testing of SATD Material |  |  |  |  | Material Verification |
| --- | --- | --- | --- | --- | --- |
| Project Engineer to submit verification samples of Common Borrow. | 1 | per | 15000 | Cubic Yard |  |
| 35 LBS in a Soils Bag |  |  |  |  |  |
| Project Engineer to submit verification samples of material of Capping Borrow. | 1 | per | 15000 | Cubic Yard |  |
| 35 LBS in a Soils Bag |  |  |  |  |  |
| Project Engineer to submit verification samples of material of Modified Borrow. | 1 | per | 15000 | Cubic Yard |  |
| 35 LBS in a Soils Bag |  |  |  |  |  |
| Project Engineer to submit verification samples of material of Select Borrow. | 1 | per | 15000 | Cubic Yard |  |
| 35 LBS in a Soils Bag |  |  |  |  |  |
| Project Engineer to submit verification samples of Clay Core material. | 1 | per | 15000 | Cubic Yard |  |
| 35 LBS in a Soils Bag |  |  |  |  |  |
| Project Site Testing |  |  |  | Material | Sampling and Testing |
| Compaction and Moisture analysis of Common Borrow to | 4 | per | 1 | Lane Mile per Lift |  |
| be performed by Project Engineer. Submit Compaction report, Form OMT 161 (both pages) or OMT 031 to MMD for clearance. | 1 | per | 2000 | Cubic Yard |  |
| Compaction and Moisture analysis of Capping Borrow to | 4 | per | 1 | Lane Mile per Lift |  |
| be performed by Project Engineer. Submit Compaction report to MMD for clearance. | 1 | per | 2000 | Cubic Yard |  |
| Compaction and Moisture analysis of Modified Borrow to | 4 | per | 1 | Lane Mile per Lift |  |
| be performed by Project Engineer. Submit Compaction report to MMD for clearance. | 1 | per | 2000 | Cubic Yard |  |
| Compaction and Moisture analysis of Select Borrow to be | 4 | per | 1 | Lane Mile per Lift |  |
| performed by Project Engineer. Submit Compaction report to MMD for clearance. | 1 | per | 2000 | Cubic Yard |  |

Compaction and Moisture analysis of Select Borrow for Trench Backfill to be performed by Project Engineer.

Submit Compaction report to MMD for clearance.

Compaction and Moisture analysis of Clay Core material to be performed by Project Engineer. Submit Compaction report to MMD for clearance.

# Soil Materials, Furnished Landscaping Soils

1  per	150	Linear Feet per 3 Foot Lift

1  per	2000	Cubic Yard

## Plant or Product Qualification

Evaluation of Production Facility for SATD Materials	Facility Qualification

Material Producer to have their soil product tested by an independent laboratory and submit results to SATD.

1  per	6	Months

Evaluation of Material Product for SATD Materials	Product Qualification

Quality Evaluation of Furnished Topsoil Product.

20 LB in a Soils Bag

1  per	1	Prior to Source Approval

1  per	6	Months

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

Material Verification for SATD Materials	Material Verification

Project Engineer to verify material and submit the approved Form 27B to the Materials Management Division for clearance. Form 27B may be found on the Documents Tab on the material source submission.

# Soil Materials, Salvaged & Other Landscaping Soils

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

SATD Material Review	Material Certification for Project Usage

Project Engineer to contact SATD at least 30 days prior to material usage or placement. SATD will sample material at source, ensure material testing, and provide a Soil Test Report (Form 27B) and the Nutrient Management Plan.

20 LB in a Soils Bag

Project Engineer to contact SATD at least 30 days prior to material usage or placement. SATD will sample material at source, ensure material testing, and provide a Soil Test Report (Form 27B).

20 LB in a Soils Bag

1  per	1	Prior to Usage on Project

1  per	1	Prior to Usage on Project

## Project Construction

Material Verification for SATD Materials	Material Verification

Project Engineer to verify material and submit the approved Form 27B to the Materials Management Division for clearance.

# Soil Stabilization Matting

1  per	1	Item Completion

## Plant or Product Qualification

Evaluation of Material Producer for LPD Materials	Facility Qualification

Production facility data maintained to track the material supply chain and provide a basis for qualified products.

1  per	1	Prior to Source Request

Evaluation of Material Producer for LPD Materials	Product Qualification

Qualification of Material Product for use on State Projects	1  per	1	Prior to Usage on Project

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

LPD Material Verification	Material Verification

Project Engineer to visually inspect soil stabilization matting and fasteners during installation. Project Engineer to visually inspect placed material after installation.

# Surface Treatments

1  per	1	Delivery to Project

## Plant or Product Qualification

Evaluation of Production Facility for ATD Materials	Facility Qualification

Production facility data maintained to provide a basis for qualified products.

.

1  per	1	Prior to Source Request

Evaluation of Material Product for ATD Materials	Product Qualification

Review and Qualification of Material Mixture for use on State Projects.

.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

Notification of Production for ATD materials	Production Notification

Producer to notify the Asphalt Technology Division one week prior to material placement.

.

1  per	1	Placement Day

## Project Construction

ATD Material Verification	Material Verification

Project Engineer to collect material certifications (TC 1.03 w/o test results) and submit to materials management for clearance.

.

1  per	1	Delivery to Project

Sampling and Testing of ATD materials	Material Sampling and Testing

Project Engineer to sample emulsion and mixture. Sample to be delivered to OMT for verification.

1 Gallon of Mixture and 1 Gallon of Emulsion in a Widemouth Plastic Jar

# Traffic and Related Materials, Miscellaneous

1  per	1	Production Day

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

OOTS Material Verification	Material Verification

Project Engineer to submit Form 14 to the Materials Management Division confirming the product is undamaged, acceptably placed, and conforms to specification.

# Traffic Barrier End Treatments

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Producer (QPL)	Facility Qualification

Production facility data maintained to provide a basis for qualified products.

1  per	1	Prior to Source Request

Review of Product (QPL)	Product Qualification

Qualification of Material Product for use on State Projects.	1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

Approval of Material Prior to Shipment	Material Certification for Project Usage

Contractor to submit "Request to use NCHRP-350 Product" to the Engineer of Record. The Engineer of Record refers to a Project's design Engineer or plan sheet approver who is a Licensed Engineer in the field of design and MASH implementation.

1  per	1	Prior to Usage on Project

## Project Construction

OOTS Material Verification	Material Verification

See source response for "Metal Traffic Barrier, Certified Installer" for this item for acceptance procedures.

Project Engineer to collect manufacturer's certification (TC 1.03 w/o test data) and submit certifications to the Materials Management Division for clearance.

# Traffic Control Materials, Qualified

1  per	1	Delivery to Project

1  per	1	Delivery to Project

## Plant or Product Qualification

Review Producer (OOTS)	Facility Qualification

Production facility data maintained to track the material supply chain and provide a basis for qualified products.

1  per	1	Prior to Source Request

| Review Product (OOTS) |  | Product Qualification |
| --- | --- | --- |
| Qualification of Material Product for use on State Projects. | 1 per 1 | Prior to Source Request |
| Source Approval |  |  |
| Source Submission |  | Source of Supply Submittal |
| Source of Supply Processing | 1 per 1 | Prior to Usage on Project |

## Project Construction

OOTS Material Verification	Material Verification

Project Engineer to collect certifications (TC 1.03 w/o test data) and submit certs to the Materials Management Division for clearance.

# Traffic Control Materials, Qualified & Temporary

1  per	1	Delivery to Project

## Plant or Product Qualification

Review Producer (OOTS)	Facility Qualification

Production facility data maintained to track the material supply chain and provide a basis for qualified products.

1  per	1	Prior to Source Request

Review Product (OOTS)	Product Qualification

Qualification of Material Product for use on State Projects.	1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

OOTS Material Verification	Material Verification

Project Engineer to submit Form 14 to the Materials Management Division confirming the product is undamaged, acceptably placed, and conforms to specification. Indicate the product manufacturer and model number (when available).

# Traffic Control Materials, Specialty Items

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

Review Product (OOTS)	Product Qualification

Product data maintained for historical purposes.	1  per	1	Prior to Usage on Project

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

Approval of Material Prior to Shipment	Material Certification for Project Usage

Producer to submit Shop Drawings or Catalog Cuts to the Office of Traffic and Safety for evaluation.

1  per	1	Prior to Usage on Project

## Project Construction

OOTS Material Verification	Material Verification

Project Engineer to submit Form 14 to the Materials Management Division confirming receipt of approved documentation from OOTS and conformance to specifications.

# Traffic, Misc. Services and Products

1  per	1	Delivery to Project

## Plant or Product Qualification

Review Producer (OOTS)	Facility Qualification

Facility data maintained to provide a basis for product data or historical reference.

1  per	1	Each

Review Product (OOTS)	Product Qualification

Product data maintained for historical purposes.	1  per	1	Each

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Project Construction

OOTS Material Verification	Material Verification

Project Engineer to submit Form 14 to the Materials Management Division confirming the product is undamaged, acceptably placed, and conforms to specification. Indicate the product manufacturer and model number (when available).

# Water, Pesticides, and Adjuvants

1  per	1	Delivery to Project

## Plant or Product Qualification

Review of Misc Production Location	Limited Producer Check

Production facility data maintained to track the material supply chain.

1  per	1	Prior to Source Request

## Source Approval

Source Submission	Source of Supply Submittal

Source of Supply Processing	1  per	1	Prior to Usage on Project

## Material Production

LPD Material Review	Material Certification for Project Usage

Project Engineer to contact LPD to ensure that pesticides and pesticide application methods meet specifications. An Integrated Pest Management Plan (IPM Plan) or Integrated Pest Management Form (IPMF) may be required for approval by LPD.

1  per	1	Prior to Usage on Project

## Project Construction

Visual Inspection of Placed Material	Material Sampling and Testing

Project Engineer to inspect placed material. Project Engineer to submit Form 14 for material clearance.

1  per	1	Item Completion