CATEGORY 500

PAVING

SECTION 520 — PLAIN AND REINFORCED PORTLAND CEMENT CONRETE PAVEMENTS

520.03.06 Reinforcement.

DELETE:  The first paragraph.

INSERT:  The following.

520.03.06 Reinforcement.  Reinforcement shall be as specified.  Dowel bars are smooth round bars which serve as load transfer devices across transverse concrete joints to allow concrete slab contraction and expansion, regardless of whether they are designated by bar number or diameter.  Refer to Standard MD 572.21 for dowel bar sizes and requirements.  Refer to Standard MD 572.23 for dowel bar assembly.  Tie bars are deformed rebars or connectors used for holding together longitudinal concrete joints, regardless of whether they are designated by bar number or diameter.

Maintain the reinforcement in a clean condition, free from foreign material that may prevent proper bonding of the concrete. Secure all reinforcement to prevent displacement or movement.

520.03.07 Concrete Placement.

DELETE:  The fourth paragraph, “Single Layer Placement…specified in 917.02.”

INSERT:  The following.

Single Layer Placement.  Set the reinforcement on chairs capable of maintaining the stability and proper elevation of the reinforcement. Welding of reinforcement to the chairs in lieu of wire ties will be permitted, except welding for epoxy-coated reinforcement will be permitted only if the epoxy coating is applied after the welding.  Refer to Standard MD 572.23 for welding restrictions of dowels.  Repair damage to epoxy coating using materials specified in 917.02.

520.03.12 Curing.

DELETE:  The first paragraph.

INSERT:  The following.

520.03.12 Curing. Following texturing and edging, cure the concrete for at least 72 hours. Whenever the ambient air temperature falls below 40 F during the curing period, use insulated or electric blankets, or a method approved by OMT, to maintain the concrete temperature above 40 F and extend cure time to at least 96 hours for cold weather applications. Use the methods described above in addition to any curing material that is used. Provide a sufficient number of high/low thermometers to monitor the temperature of the concrete. Cure the concrete using one of the following methods: