CATEGORY 900

MATERIALS

SECTION 901 — AGGREGATES

DELETE:  Table 901 D in its entirety.

INSERT:  The following.

TABLE 901 D

AGGREGATE PHYSICAL PROPERTY REQUIREMENTS FOR ASPHALT MIXES

| MATERIAL | S P E C I F I C A T I O N | TEST METHOD |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | T 11 | T 96 | T 104 | D 4791 | MSMT 216 |
|  |  | MATERIAL FINER THAN No. 200 SIEVE % max | LOS ANGELES ABRASION (LA) % max | SODIUM SULFATE SOUNDNESS % max | FLAT and ELONGATED (a) % max | DYNAMIC FRICTION VALUE (DFV) (b) (c) min |
| SURFACE COURSE 4.75 mm, 9.5 mm, 12.5 mm, and 19.0 mm | M323 | — | 45 | 12 | 10 | 25 |
| SURFACE COURSE — HIGH DFV 4.75 mm, 9.5 mm, 12.5 mm, and 19.0 mm | M323 | — | 45 | 12 | 10 | 40 (e) |
| BASE COURSE 19.0 mm, 25.0 mm and 37.5 mm | M323 | — | 45 | 12 | 10 | — |
| GAP GRADED STONE MATRIX ASPHALT 9.5 mm, 12.5 mm, and 19.0 mm | M323 | — | 30 | 12 | 20/5 (g) | 40 (e) |
| OPEN GRADED FRICTION COURSE 9.5 mm, 12.5 mm, 12.5 mm PEM (h) | MSMT 409 | 0.5 | 30 | 12 | 20/5 (g) | 40 (e) |
| SLURRY SEAL (SS) and MICRO-SURFACING (MS) | — | — | — | 12 | — | 40 (f) |
| CHIP SEAL SURFACE TREATMENT | M 80, CLASS A | 1.0 (d) | 45 | — | — | — |

- Testing for flat and elongated particles shall be conducted on the blended aggregates.   Dimensional ratio of calipers shall be 5:1.

- The minimum Dynamic Friction Value (DFV) shall be based on a single aggregate source or a blend of aggregates used.  Determine proportions of blended aggregates using MSMT 416.

- DFV determined on parent rock.  Reclaimed asphalt pavement (RAP) shall have a DFV of 30.0.

- 1.0 for samples taken at the point of production.  Samples taken at any point after shipment shall have no more than 1.5 percent finer than 0.075 mm sieve.

- Carbonate rock shall have a minimum of 25 percent insoluble residue retained on the 0.075 mm sieve.

- No blending allowed.

- Testing conducted on particles retained on the 4.75 mm sieve. Dimensional ratio of calipers shall be 3:1/5:1.

- Porous European Mix.