CATEGORY 900

MATERIALS

SECTION 920 — LANDSCAPING MATERIALS

920.01.01 Existing Topsoil and Salvaged Topsoil.

920.01.01(c) Composition.

DELETE:  The table in its entirety.

INSERT:  The following.

| COMPOSITION - EXISTING TOPSOIL & SALVAGED TOPSOIL |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| TEST PROPERTY | TEST1 METHOD | TEST VALUE AND AMENDMENT |  |  |  |
| Prohibited Weeds | — | Free of live stems or roots of Shattercane, Johnsongrass, Canada Thistle, Bull Thistle, Plumeless Thistle, Musk Thistle, Common Reed and Japanese Knotweed when inspected before transportation. |  |  |  |
| Debris | — | 1.0 percent or less by weight of cement, concrete, asphalt, crushed gravel or construction debris when inspected. |  |  |  |
| Grading Analysis | R-58 | Sieve Size |  | Passing by Weight Minimum % |  |
|  |  | 2 in. |  | 100 |  |
|  |  | No. 4 |  | 90 |  |
|  |  | No. 10 |  | 80 |  |
| Textural Analysis | T-88 | Particle |  | % Passing by Weight |  |
|  |  | Size | mm | Minimum | Maximum |
|  |  | Sand | 2.0 – 0.050 | 15 | 77 |
|  |  | Silt | 0.050 – 0.002 | Combined Silt and Clay 23 | 80 |
|  |  | Clay | less than 0.002 |  | 30 |
| Soil pH | ASTM D 4972 | pH of 4.8 to 7.6. Apply limestone to Existing Topsoil and Salvaged Topsoil with pH 4.8 to 6.1 per NMP. Apply sulfur to Existing Topsoil and Salvaged Topsoil with pH 7.1 to 7.6 per NMP. |  |  |  |
| Organic Matter | T-267 | 1.0 to 8.0 percent OM by weight. Apply compost to Existing Topsoil and Salvaged Topsoil with 1.0 to 3.7 percent OM per NMP. |  |  |  |
| Nutrient Content | — | Administration will assess. Apply fertilizer per NMP for nitrogen requirement and optimum fertility index values (FIV) for phosphorus and potassium. |  |  |  |
| Soluble Salts | EC 1:2 (V:V) | 800 ppm (1.25 mm hos/cm) or less. Apply gypsum to Existing Topsoil and Salvaged Topsoil with 500 to 800 ppm (0.78 to 1.25 mhos/cm) per NMP. |  |  |  |
| Harmful Materials | — | Topsoil shall not contain substances in concentrations that are harmful to human health, water quality, or plant growth. Industrial waste such as ash, slag, raw sludge, or similar materials shall not be soil components. |  |  |  |
| Note: 1 Materials Standards and Materials Testing 356 (MSMT 356) has been superseded by OMT Landscaping Soils Eligibility List. Test methods not defined herein shall be as per visual inspection or methods defined by the Landscape Operations Division. |  |  |  |  |  |