CATEGORY 900

MATERIALS

DELETE:  SECTION 926 — RESERVED.

INSERT:  The following.

SECTION 926 — FOAMED ASPHALT STABILIZED BASE COURSE MIX

926.01 Mix Requirements. Develop a mix consisting of Reclaimed Asphalt Pavement (RAP), Recycled Portland Concrete (RC), aggregate, and foamed asphalt binder.  Include lime, Portland cement, and fly ash as necessary to increase the fines to meet the design parameters in Table 1 and Table 2. Select a PG 64-22 asphalt binder that provides the required asphalt foaming characteristics and mix properties.  Do not use polymer modified asphalt binders.

Table 1 - Aggregate Blend Requirements

| GRADATION (T 27) |  |
| --- | --- |
| Sieve Size | Percent Passing |
| 1 ½ in (38 mm) | 100 |
| ¾ in (19 mm) | 65 – 100 |
| No. 4 (4.74 mm) | 50 – 70 |
| No. 200 (75 µm) | 1 – 8 |
| OTHER |  |
| PI (T 90) | < 10 % |

Table 2 - Foamed Asphalt Stabilized Base Course Mix Requirements

| DESIGN PARAMETERS | VALUE |
| --- | --- |
| Aggregate Blend Compaction: T 180D, Max Dry Density, pcf | ≥120 |
| Specimen compaction: Marshall compaction: T 245 - number of blows per face, or Gyratory compaction: T 312 - number of gyrations |  |
|  | 75 |
|  | 30 |
| Indirect Tensile Strength: modified T 283 Minimum Wet Tensile Strength, psi Minimum Wet Tensile Strength, psi, for material stockpiled >2 days Minimum Tensile Strength Ratio (TSR), % |  |
|  | 45 |
|  | 55 |
|  | 70 |
| Foamed Asphalt Expansion Characteristics @ 160, 170, & 180 C Minimum Half-Life of Foamed Expansion, sec (1) Minimum Expansion Ratio (2) |  |
|  | 8 |
|  | 10 |

- Total time for foamed asphalt to settle to half of the maximum foamed volume. See Section A.1.3.4 of the Wirtgen Cold Recycling Technology Manual (2010) for the half-life test procedure. Alternate suitable equipment can be substituted for the Wirtgen WLB 10 S laboratory unit.

- Maximum foamed asphalt volume divided by non-foamed asphalt volume. See Section A.1.3.4 of the Wirtgen Cold Recycling Technology Manual (2010) for the expansion ratio test procedure. Alternate suitable equipment can be substituted for the Wirtgen WLB 10 S laboratory unit.

Submit job mix formulas for approval at least 30 days prior to production to the Office of Materials Technology, Soils and Aggregate Division. Job mix formulas must meet the requirements of Table 1 and Table 2. Work will not be allowed to commence without approved job mix formulas. Perform the following tests for each job mix formula:

- Aggregate.  T 2.  Sample 50 lb of material representing the RAP, RC, and aggregate to be used in the job mix formula.  Test per 901A and 901B.

- Performance Graded Asphalt Binder.  M 322. Provide five 4-quart samples of the asphalt binder.

- Water. 921.01

- Lime, Cement and Fly Ash.  Determine the percentage of lime, cement and fly ash required to meet the mix design parameters

926.02 Mix Design.  Prepare a minimum of 4 Marshall or 4 gyratory compactor specimens at 0.5 percent increments for a range of asphalt contents; with at least one specimen above and one below optimum to determine the job mix formula.  The moisture content of the specimens shall be within 1.5 percent of the optimum moisture content of the aggregate blend.  For gyratory specimens, obtain a 2 in. thick test specimen cut from the middle of each compacted cylinder.

926.03 Foamed Asphalt Expansion Characteristics. Test the asphalt binder per Table 2 for the following:

- Measure the expansion ratio and foam half-life of the asphalt binder over a range of water contents for the three temperatures.

- Plot expansion ratio and half-life vs. water content. The optimum foaming water content for a given temperature is the average of the two water contents that meet the respective minimum expansion ratio and half-life requirements.

926.04 Indirect Tensile Strength (IDT).   T 283.

- Place the samples to be soaked in a 77 F water bath for 24 hours. Dry the samples to constant mass at 104 +/-2 F.

- Graph IDT strength versus foamed asphalt content for both dry and soaked specimens. Graph TSR versus foamed asphalt content.

- For wet IDT strength vs. foamed asphalt content curves exhibiting a maximum value, select the design foamed asphalt content corresponding to the maximum. Otherwise, select a design foamed asphalt content that meets the wet IDT strength and TSR requirements in Table 2.

- In no case shall the design foamed asphalt content be less than 2 percent or greater than 3.5 percent.

926.05 Foamed Asphalt Cement Content. Once the foamed asphalt content of the Job Mix Formula has been determined, prepare a minimum of 5 compacted specimens based on the Job Mix Formula. These specimens must meet the design parameters per Table 2. Calculate the mean, standard deviation of the Indirect Tensile Strength results (modified T 283, per Table 2). These values must be reported in the FASBC Mix Design for the Administration’s approval.

The Contractor shall also submit 5 bag samples representative of the aggregate blend of the Job Mix Formula and 5 bag samples representative of the Job Mix Formula with the added foamed asphalt as part of the mix approval process. These sample bags shall contain at least 20 lb of FASBC material. The samples will be tested to develop an ignition oven correction factor and a base reference for the foamed asphalt cement content for acceptance purposes.

The Office of Materials Technology will evaluate the suitability of the material and proposed job mix formula. If the job mix formula is not approved, submit a new job mix formula as directed.