CATEGORY 900

MATERIALS

SECTION 927 — OPEN GRADED FRICTION COURSE

Open Graded Friction Course (OGFC) shall conform to the applicable sections of 901 and PP 77, except as specified.

GRADATION:

| Sieve Size | Mixture Control Tolerance, % | Design Gradation Limits, % Passing |  |  |
| --- | --- | --- | --- | --- |
|  |  | 9.5 mm OGFCa | 12.5 mm OGFCa | 12.5 mm PEMb |
| 3/4 in. (19 mm) | ±0.0 |  | 100* | 100* |
| 1/2 in. (12.5 mm) | ±6.0 | 100* | 85-100 | 80-100 |
| 3/8 in. (9.5 mm) | ±5.5 | 85-100 | 55-75 | 35-60 |
| No. 4 (4.75 mm) | ±6.0 | 20-40 | 15-25 | 10-25 |
| No. 8 (2.36 mm) | ±4.5 | 5-10 | 5-10 | 5-10 |
| No. 200 (75 µm) | ±2.0 | 2-4 | 2-4 | 1-4 |
| Range for % AC | ±0.4 | 6.0-7.25 | 5.75-7.25 | 5.5-7.0 |
| Drain-down (D6390), %c |  | <0.3 | <0.3 | <0.3 |

*Mix Control Tolerance not applicable to this sieve for this mix.

- Less than Design Level 4 (ESAL).

- Porous European Mix (PEM) – Design Level 4 (ESAL).

- Conduct drain-down test on loose mix at a temperature 15 C higher than anticipated production temperature.

Crushed glass, roofing shingles, RAP, or other recycled materials are not allowed in OGFC mixes.

PHYSICAL PROPERTIES:

| TEST | TEST METHOD | LIMITS |
| --- | --- | --- |
| Asphalt Bindera | M332 | 64E-22 |
| Tensile Strength Ratio (TSR) | T283b | ≥85% |
| Permeabilityc | MSMT 408 | 300 ft/day (100m/day) |

- Mineral Fibers used at 0.4% of total mix, Cellulose, 0.3% of total mix, or other approved stabilizer systems as specified in 904.05.04.

- Tensile Strength Ratio using T 283 with the following exceptions:

  - Compact using 50 gyrations of a Superpave gyratory compactor.

  - Apply partial vacuum of 26 in. (660 mm) Hg for 10 minutes to whatever saturation level is achieved.

  - Use five freeze/thaw cycles, keeping the specimens submerged in water during the freeze cycles.

- Permeability is required when material is to be used in Porous Asphalt Pavement Systems.