CATEGORY 900

MATERIALS

(Use SP 559 POLYUREA PAVEMENT MARKINGS in conjunction with this Specification.)

SECTION 951— POLYUREA PAVEMENT MARKING MATERIALS

# ADD:  The following after 951.09.

951.10 POLYUREA PAVEMENT MARKING MATERIALS.  Polyurea pavement marking materials shall consist of a 100 percent solids two-component system.

951.10.01 Physical Components

- Composition.  The polyurea coating shall be formed by the reaction of two components (Part A and Part B).

- At least one component shall be composed of secondary amines, pigments and fillers as needed to meet performance requirements of this specification.

- The two components shall be formulated so they cure properly cure when mixed at a volumetric ratio of two volumes of Part A and one volume of Part B (2:1).

- The components shall not contain appreciable amounts of volatile diluents. The polyurea coating shall be essentially a 100 percent solids product.

- The polyurea coating materials shall be manufactured without the use of lead chromate pigments or other similar, lead-containing chemicals.

- The white polyurea shall contain not less than 16 percent by weight rutile titanium dioxide pigment to ensure adequate opacity, hiding power and reflective properties.

Store the binder components in a cool, dry, well ventilated area indoors 40 F to 100 F (4 C to 38 C).  Use within 12 months of receipt.

- Pigment.  D 476.

- Component A - White shall consist of Type II Rutile Titanium Dioxide only.  No extender pigments are permitted.

- Component A - Yellow shall consist of yellow pigments and tinting colors proportioned to produce the color specified in 951.10.03(b). Titanium dioxide used in Component A -Yellow shall conform to Type II Rutile.

951.10.02 Restrictions.  The combined total of heavy metals listed in CFR 40, Section 261.24, Table 1, shall not exceed 100 ppm when tested by X-Ray Fluorescence, ICP, or comparable method capable of this level of detection.

951.10.03 Mixed Composition.

- Mixing Ratio.  The ratio for mixing the polyurea pavement marking material according to the manufacturer's recommendations is 2:1.   The ratio shall not vary more than 2.5 percent.

(b)	Color - White and Yellow:

- Production.  The color of the cured production polyurea material film of the production sample shall match the specified color chips conforming to Federal Standard 595 when compared visually or by instrumental measurement.

- Control.  Control color matching determinations will be made using a Pacific Scientific Color Machine at an observation angle of 2 degrees, and the C.I.E. Chromatically Coordinate Color Matching System under light source Illuminate C, with the following tolerances permitted between the standard chip and the cured epoxy film sample:

|  | # WHITE # Color No. 37925 |  | # YELLOW # Color No. 38907 |  |
| --- | --- | --- | --- | --- |
|  | X | Y | X | Y |
| Standard Chip | 0.310 | 0.330 | 0.480 | 0.450 |
| Delta Tolerance | ± 0.020 | ± 0.020 | ± 0.030 | ± 0.030 |

951.10.04 Color and Weathering Resistance:  The mixed polyurea compounds, both white and yellow, when applied to 3 in. x 6 in. aluminum panels at 15 1 mil in thickness with no glass beads or elements and exposed for 500 hours in a Q.U.V. Environmental Testing Chamber, as described in ASTM-G154, Cycle #1, shall conform to the minimum requirements. Color shall not change appreciably.

# 951.10.05 Track-Free Time.  D711. The polyurea marking material shall reach a track-free condition in 10 minutes or less for a 15 mil thickness when tested as specified.  The track-free time shall not increase substantially with temperature decreasing to 30 F.

# 951.10.06 Adhesion to Concrete.  ACI Method 503.  The polyurea coating shall have such a high degree of adhesion to the concrete test specimen that the specimen shall exhibit a substantial failure when tested.  The prepared specimens shall be conditioned at room temperature (75 F 2 F) for a minimum of 24 hours and maximum of 72 hours prior to testing.

951.10.07 Adhesion to Asphalt.  ACI Method 503.  The polyurea coating shall have such a high degree of adhesion to the asphalt test specimen that the specimen shall exhibit a 100 percent failure when tested. The prepared specimens shall be conditioned at room temperature (75 F  2 F) for a minimum of 24 hours and maximum of 72 hours prior to testing.

951.10.08 Qualification.  Manufacturers desiring to have their materials approved for Administration use shall have their products evaluated on either a NTPEP Northern Test Deck, a

test deck in Maryland or other state’s test deck data unless otherwise waived. Modifications to previously approved products may be accepted for qualification. The Office of Materials Technology will determine qualification.

951.10.09 Material Acceptance.  The manufacturer shall provide access to the Administration’s representative for collecting samples from each production batch prior to shipment. The samples shall be sent to the Administration’s laboratory for QA testing.  Each sample shall be accompanied by certification per TC-1.03 and as specified. Production batch samples will be subject to random tests, such as but not limited to, X-ray spectroscopy, infrared spectroscopy, ultraviolet spectral analysis, and atomic absorption spectroscopy. The Administration will determine conformance with the requirements.   Approval will be required before a batch or a portion of a batch is shipped.

Take random samples on the project in conformance with the Frequency Guide of the Materials Quality Assurance Manual and test as specified. Non-conformance may result in the suspension from the certification program until qualification is reestablished.

951.10.10 Certification.  The manufacturer shall certify that any pavement marking batch supplied conforms to all specifications in TC-1.03 and provide a statement certifying that any paint supplied is identical in composition to the material submitted for NTPEP testing.  The same code name used on the test deck must identify the product.  Failure to certify will be grounds for product batch rejection.

Certification shall also include the following:

- Manufacturer’s name.

- Manufacturer’s address.

- Material color.

- Manufacture date (mm-dd-yy).

- Lot or batch identification number.

- Lot/batch size.

(g) Material Safety Data Sheets.

951.10.11 Production Facility

- The manufacturer shall provide a facility capable of producing thermoplastic pavement markings in the quantity and quality specified; subject to Administration approval.

- The manufacturer shall provide a laboratory capable of performing the required tests, subject to Administration approval.

951.10.12 Packaging.  Label each container with the following:

- Manufacturer's Name.

- Manufacturer’s address.

- Material color and component type, if applicable.

- Manufacture date (mm-yy).

- Lot or batch identification number.