CATEGORY 400

STRUCTURES

SECTION 440 — Prestressed Concrete Beams and Slab Panels

440.02 MATERIALS

DELETE:  440.02.05 in its entirety.

440.03 CONSTRUCTION

440.03.20 Erection.

DELETE:  Subsection (g) in its entirety.

INSERT:  The following.

(g)	Grout the shear keys by overfilling the joints. Drive the grout or compactly tamp it into the keyways; do not vibrate. After 5 minutes, strike off the excess grout flush with the top of the panels. Follow the manufacturer’s recommendations for grouting in cold or hot weather.

DELETE:  Subsection (k) in its entirety.

INSERT:  The following.

- Allow a minimum of 24 hours between grouting of shear keys and final tensioning of lateral tie rods provided temperature is 70 F and above when shear key grout is placed.  If temperature is below 70 F during the initial 24 hours, cure for a total of 72 hours or per the approved manufacturers specifications.  Contractor has the option to provide cold weather protection to ensure temperature does not fall below 70 F during the initial 24 hours.

440.03.21 Bearing Pads.

DELETE:  The first sentence in the second paragraph, “Coat the surfaces… epoxy adhesive.”

INSERT:  The following.

Coat the surfaces of the concrete bearing areas that will be in contact with the bottom of the bearing pads and the full contact area of the bottom of the bearing pads with epoxy adhesive.

DELETE:  440.03.22 in its entirety.

INSERT:  The following.

440.03.22 Placing and Finishing Concrete Overlay.  Place and finish the overlay as specified in 420.03 including superstructure placement restrictions.

Unless otherwise noted on the contract plans, place the entire bridge slab overlay in one continuous pour.  No transverse or longitudinal joints will be permitted.

Place the finishing machine’s supporting rails outside the overlay limits.  Do not use hold down devices that are shot or drilled into the concrete.  Submit plans for anchoring support rails and the concrete placing procedure for approval.

Take precautions to secure a smooth riding surface as specified in 420.03.07(d).  Prior to placement operations, review the equipment, procedures, and personnel with the Engineer.  Place the concrete overlay using the following sequence of operations.

- Placement of the overlay may occur once the parapet and curbs have cured for 24 hours. Concrete curbs and parapets may be placed once the lateral tie rods have been tensioned to the final tensioning force and the shear key grout has met the curing requirements.

- Before placing the reinforcing steel mat, thoroughly clean and water blast the entire surface that will be in contact with the overlay then clean the surface with air blast.

- Place and tie the support chairs to the underside of the reinforcing mat to locate the reinforcing mat 2 1/2 in. clear of the top of the deck overlay .

- Set-up the finishing screed and make a dry run of the finishing operation to verify that the reinforcing is properly located and the finished deck elevation shown on the plans can be achieved.

- Prior to concrete placement, air blast the surface to receive the overlay to remove any foreign material that may have collected since the water blasting.  Following the air blast, moisten the entire surface with a misting operation for at least 1 hour immediately prior to  the placement of the concrete overlay.  Keep the top surface of the prestressed slabs moist until the placement of the overlay and throughout the placement operation and remove any puddling of water prior to and throughout the concrete placement.

- Allow no vehicular traffic on the prepared deck surface before overlay placement.