CATEGORY 900

# MATERIALS

# SECTION 911 — Joints

911.06 SEALER FOR LOOP DETECTOR

911.06.01 Tests.

DELETE:  The Table.

INSERT:  The following.

| TYPE A – TWO PART EPOXY |  |  |
| --- | --- | --- |
| TEST PROPERTY | TEST METHOD | SPECIFICATION LIMITS |
| Viscosity, cone and plate Viscometer@ 25 C, cps max | — | 12 000 |
| Pot life @ 25 C, minutes min | — | 10 |
| Cure time @ 25 C, no tackiness, hr max | — | 1 |
| Hardness, Type D durometer | D 2240 | 50 – 60 |
| Tensile elongation, % min | D 638 | 100 |
| Water absorption, %/24 hr max | D 570 | 0.5 |
| Oil absorption, % max | D 471 | 0.02 |
| Volume resistivity @ 25 C, ohm-cm min | D 257 | 2.4 X 1010 |
| TYPE B - ONE PART POLYURETHANE |  |  |
| TEST PROPERTY | TEST METHOD | SPECIFICATION LIMITS |
| Viscosity, Brookfield RVF #6 spindle @ 20 rpm 25 C, cps max | — | 30 000 |
| Cure time @ 25 C, no tackiness, hr max | — | 24 |
| Hardness, Rex Type A | — | 50 – 60 |
| Tensile strength, psi min | D 412 | 500 |
| Tensile elongation, % min |  | 300 |
| ARC resistance, sec min | D 495 | 70 |
| Dielectric constant, min | D 150 | 6 @ 50 hz 4.25 @ 500 kHz |
| Nonvolatile content, % | — | 85 |