# Category 900

# MATERIALS

# SECTION 912 — Coating Systems for Structural Steel

##### 912.02 PRIMER COATS AND SEALERS

##### DELETE:  912.02.05 and 912.02.06 in its entirety.

INSERT:  The following.

912.02.05 Penetrating Sealer.  Shall have a viscosity of 75 to 101 KU and be able to penetrate and seal existing coatings and substrate.  It shall be suitable for application over marginally prepared steel and most generic types of aged coatings.  The sealer shall conform to one of the following:

- Epoxy penetrating sealer shall be cross-linked amido-amine epoxy primer/sealer having two components mixed in accordance with the manufacturer’s recommendations. It shall be a minimum of 95 percent solids by weight.

(b) Moisture cured urethane micaceous iron oxide filled penetrating primer/sealer shall be one component having a minimum of 75 percent solids by weight.  It shall also meet the Moisture Cured Urethanes Additional Performance Criteria Table.

##### 912.03 INTERMEDIATE COATS

##### DELETE:  912.03.03 in its entirety.

##### 912.04 FINISH COATS

##### DELETE:  912.04.03 in its entirety.

INSERT:  The following.

912.04.03 Polyaspartic Urethane.  Finish coat shall have a solids of 75-85 percent by weight and 65-75 percent by volume.  Drying time to touch and hard shall be the minimum recommended by the paint manufacturer.

##### 912.05  PAINT SYSTEMS

##### DELETE:  912.05 in its entirety.

INSERT:  The following.

## 912.05 PAINT SYSTEMS

As specified in the Paint Systems Table.

| PAINT SYSTEMS TABLE |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| PAINT | COAT | SECTION | DRY FILM THICKNESS, mils, min - max | USAGE |  |
| SYSTEM A |  |  |  |  |  |
| Inorganic Zinc | I | 912.02.01 | 3.0 - 5.0 | Shop Primer Coat |  |
| Acrylic | II | 912.03.01 | 2.0 - 4.0 | First Intermediate Coat |  |
| Acrylic | III | 912.04.01 | 2.0 - 4.0 | Finish Coat |  |
| SYSTEM B |  |  |  |  |  |
| Inorganic Zinc | I | 912.02.01 | 3.0 - 5.0 | Shop Primer Coat |  |
| Epoxy Polyamide | II | 912.03.02 | 5.0 - 8.0 | Intermediate Coat |  |
| Aliphatic Urethane | III | 912.04.02 | 2.0 - 3.0 | Finish Coat |  |
| SYSTEM C |  |  |  |  |  |
| Organic Zinc | I | 912.02.03 | 3.0 - 5.0 | Primer Coat |  |
| Epoxy Polyamide | II | 912.03.02 | 5.0 - 8.0 | Intermediate Coat |  |
| Aliphatic Urethane | III | 912.04.02 | 2.0 - 3.0 | Finish Coat |  |
| SYSTEM D |  |  |  |  |  |
| Organic Zinc | I | 912.02.03 | 3.0 - 5.0 |  | Primer Coat |
| Acrylic | II | 912.03.01 | 2.0 - 4.0 |  | Intermediate Coat |
| Acrylic | III | 912.04.01 | 2.0 - 4.0 |  | Finish Coat |

| SYSTEM E |  |  |  |  |
| --- | --- | --- | --- | --- |
| Aluminum Epoxy Mastic | I | 912.02.02 | 5.0 - 8.0 | Primer Coat |
| Epoxy Polyamide | II | 912.03.02 | 5.0 - 8.0 | Intermediate Coat |
| Aliphatic Urethane | III | 912.04.02 | 2.0 - 3.0 | Finish Coat |
| SYSTEM F |  |  |  |  |
| Zinc Rich Moisture Cured Urethane | I | 912.02.04 | 2.0-3.0 | Primer Coat |
| Polyaspartic Urethane | II | 912.04.03 | 6.0-9.0 | Finish Coat |
| SYSTEM G |  |  |  |  |
| Zinc Rich Moisture Cured Urethane | I | 912.02.04 | 2.0 - 3.0 | Primer |
| Epoxy Polyamide | II | 912.03.02 | 3.0-5.0 | Intermediate Coat |
| Polyaspartic Urethane | III | 912.04.03 | 6.0-9.0 | Finish Coat |
| SYSTEM H |  |  |  |  |
| Penetrating Sealer | I | 912.02.06 | 1.0 - 2.0 | Sealer |
| Aluminum Filled Epoxy Mastic | II | 912.02.02 | 3.0 - 5.0 | Spot Intermediate |
| Aliphatic Urethane | III | 912.04.02 | 3.0 - 5.0 | Spot Finish |
| SYSTEM I |  |  |  |  |
| ###### Organic zinc | ###### I | ###### 912.02.03 | ###### 3.0-5.0 | ###### Primer Coat |
| ###### Polyaspartic Urethane | ###### II | ###### 912.04.03 | ###### 6.0-9.0 | ###### Finish Coat |

| SYSTEM J |  |  |  |  |
| --- | --- | --- | --- | --- |
| ###### Organic Zinc | ###### I | ###### 912.02.03 | ###### 3.0-5.0 | ###### Primer Coat |
| ###### Epoxy Polyamide | ###### II | ###### 912.03.02 | ###### 3.0-5.0 | ###### Intermediate Coat |
| ###### Polyaspartic Urethane | ###### III | ###### 912.04.03 | ###### 6.0-9.0 | ###### Finish Coat |