CATEGORY 900

MATERIALS

SECTION 921 — Miscellaneous

DELETE:  921.06 TIMBER PRESERVATIVES in its entirety.

INSERT:  The following.

921.06 TIMBER PRESERVATIVES.  All preserved wood used for highway construction and maintenance applications shall be treated per M 133, and the American Wood Protection Association (AWPA) and ICC-ES standards for preservative, retention, and penetration with United States Environmental Protection Agency (EPA) pesticide registrations. Timber preservatives shall meet the following:

- Water borne preservatives shall be used where a clean surface is desired, or when the wood is to be painted. Moisture content of wood shall not be greater than 19 percent at the time of treatment.

- All treated wood shall be free of excess preservative on the surface.  Creosote-treated wood shall be double vacuum treated per EPA requirements for use in aquatic and marine environments.

- Wood used for sign posts, fence posts, wood posts, guardrail posts, bridge decking, gates, stair treads, and offset blocks shall be treated per M 133 and AWPA standards with EPA pesticide registrations.

- Wood used for piles, timbers, and composites shall be treated per M 133 and AWPA standards with EPA pesticide registrations.

- Wood used for hand-contact surfaces such as handrails, playground equipment and picnic tables shall be treated per M 133 and AWPA standards with EPA pesticide registrations for residential applications. Fasteners for preservative treated wood shall be hot-dipped galvanized steel conforming to A153 or A653, Class G185. Type 304 or 316 stainless steel fasteners are also permitted.

- Pressure treatment shall conform to the requirements of the AWPA “Use Category” as follows:

| Wood | End Use Category | AWPA Standard |
| --- | --- | --- |
| Bridge structures including decking, guard rail posts and offset blocks | UC4B - Ground Contact Heavy Duty | U1: Commodity Specification A (sawn solid products) |
| Foundation piles | UC4C - Ground Contact Extreme Duty | U1; Commodity Specification E (round timber piles) |
| Wood Composites | UC4A - Ground Contact, General Use | U1; Commodity Specification F (wood composites) |
| Sign posts, fence posts and gates | UC4A - Ground Contact, General Use | U1: Commodity Specifications A (sawn solid products) and B (round posts) |
| Piling, bracing and bulk heading | UC4B - Ground Contact Heavy Duty | U1; Commodity Specifications A (sawn solid products), B (round products) and E (round timber piles) |
| Piling, bracing, bulkheads and fender systems | UC5B Marine (Salt water) Immersion | U1: Commodity Specifications G (sawn products, round timber piles and plywood) |