CATEGORY 200

GRADING

SECTION 204 — Embankment and Subgrade

204.02 MATERIALS

ADD:  The following after 204.02.03 Embankment Adjacent to Structures.

204.02.04 Geotextile Inclusions.  Refer to 919.01 Class SD Type II Non-Woven.

204.03 CONSTRUCTION

204.03.01 Embankment Foundation

DELETE:  Paragraphs (b), “Embankment Over existing Pavement.  Thoroughly…as directed.” and (c) “Test Rolling.  When specified…or as approved.” in their entirety.

INSERT:  The following.

(b) Embankment Over Existing Pavement. When embankment is being placed in an area of existing pavement, remove the bound asphalt or concrete pavement materials prior to placing embankment material.  Leave the unbound pavement materials in place to aid in maintaining the stability of the area.

(c) Test Rolling. Unless exempted by the Engineer, test roll embankment foundation with a 35-ton pneumatic tired roller, hauling units with a weight of 35 tons, or other equipment as approved.  In case of a failed test roll, undercut unstable areas and backfill with Select Borrow or other suitable material; bridge with a thick embankment lift of Select Borrow or other suitable material and provide drainage; or other suitable treatment as determined by the Engineer at the time of construction.

Embankment foundation areas that may be exempted from test rolling include areas that do not require grubbing and areas impractical to access with test rolling equipment.

204.03.07 Subgrade.

DELETE:  The last sentence in this paragraph, “Test roll the subgrade as specified in 204.03.01(c).”

INSERT:  The following as an additional paragraph after the first paragraph:

Test roll the subgrade with a 35-ton pneumatic tired roller, or hauling units with a weight of 35 tons, or other equipment as approved.  Undercut unstable areas and backfill with Geosynthetic Stabilized Subgrade Using Graded Aggregate Base as specified in Section 211, or other specified material.

ADD:  The following after 204.03.08 Maintenance.

204.03.09 Placement of Geotextile Inclusions. Furnish and install geotextile inclusions as a compaction aid in fill embankments where the embankment is at least 10 ft high and 10 ft wide to the lines and grades shown on the Contract Documents or as directed.  Install according to the manufacturers’ recommendations.  Geotextile inclusions shall be minimum 12 ft in width.  The vertical spacing of the geotextile inclusions shall be 3 ft.  Place geotextile inclusions concurrently with the embankment material.

Unroll the geotextile onto the horizontal fill surface such that the edge of the geotextile is within 1 ft of the finished slope face.  Pull the geotextile tight prior to backfilling.  Secure the geotextile in position by suitable means according to the manufacturer’s recommendations until the subsequent soil layer can be placed.

Do not allow tracked construction equipment to operate on the exposed geotextile.  Place a minimum of 6 in. of uncompacted fill on the geotextile before operating tracked vehicles on it.  Minimize turning of tracked vehicles to prevent displacement of the geotextile or the fill.  Rubber-tired equipment may pass over the exposed geotextile at speeds of less than 10 mph.  Avoid sudden braking and sharp turns.

204.04 Measurement and Payment

DELETE:  The second and third paragraphs in their entirety.

INSERT:  The following.

204.04.01 Replacement of material lost as a result of natural causes will be measured and paid for at the Contract unit price per cubic yard for the pertinent Class of Excavation item or as directed.

204.04.02 Compaction by means of mechanical tampers or vibratory compactors will not be measured but the cost will be incidental to the pertinent Class of Excavation item.

ADD:  The following after 204.04.02, “Compaction…Excavation item.”

204.04.03 Removal of bound pavement materials will be paid for as Class 1 Excavation.

204.04.04 Geotextile inclusions will be measured and paid for at the Contract unit price per square yard of geotextile placed.

204.04.05 Undercutting will be paid for as specified in Section 201 as Class 1-A excavation.

204.04.06 Backfill will be measured and paid for as specified in Section 203.