Category 900

Materials

SECTION 902 — Portland Cement Concrete and Related Products

902.04 BLENDED HYDRAULIC CEMENT

DELETE:  902.04 BLENDED HYDRAULIC CEMENT in its entirety, “M 240 Type IP…is waived.”

INSERT:  The following.

902.04 BLENDED HYDRAULIC CEMENT

M 240 Type IP containing 15 percent to 25 percent Fly Ash by weight of blended cement, Type 1S containing 25 percent to 50 percent slag cement by weight of blended cement or Type 1L.  Maximum loss on ignition is 10.0 percent.  The requirement for a manufacturer’s written statement of the chemical composition is waived.

902.10 PORTLAND CEMENT CONCRETE

902.10.03 Portland Cement Concrete Mixtures.

ADD:  The following into Table 902 A after mix no. 12.

| M IX NO | SPECIFIED ACCEPTANCE COMPRESSIVE STRENGTH Psi | COMPREHENSIVE STRENGTH ACCEPTANCE TEST AGE days | STD. DEV. psi | CRITICAL VALUE psi | MIN CEMENT FACTOR lb/yd2 | COARSE AGGREGATE SIZE M 43/M 195 | MAX WATER/CEMENT RATIO by wt | SLUMP RANGE In. | TOTAL AIR CONTENT % | CONCRETE TEMP. F |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 13 | 4000 | 28 | 600 | 4180 | 615 | 57, 67 | 0.45 | 2 - 5 | 5 - 8 | 50 - 95 |

DELETE:  Note 1 below TABLE 902 A in its entirety, “When concrete…at 180 days.”

INSERT:  The following.

Note 1:  When concrete is exposed to water exceeding 15 000 ppm sodium chloride content, Type II cement shall be used.  In lieu of Type II cement, a Type I or a Type 1L blended hydraulic cement may be used in combined form with an amount of up to 50 percent replacement with slag cement, or an amount of up to 25 percent replacement with Class F fly ash.  The Contractor shall submit to the Engineer the proposed mix proportions and satisfactory test results according to C1012 showing a sulfate resistance expansion not exceeding 0.10 percent at 180 days.

ADD:  The following into Table 902 B after Ternary Blends.

| SCM Type | Low Alkali Cement (≤0.7% Na2O equiv.) R1 | Normal Alkali Cement (≤1.0% Na2O equiv.) R1 | Low Alkali Cement (≤0.7% Na2O equiv.) R2 | Normal Alkali Cement (≤1.0% Na2O equiv.) R2 |
| --- | --- | --- | --- | --- |
| Binary Blends with Type IL | Approval Required | Approval Required | Approval Required | Approval Required |

DELETE:  The paragraph below Table 902 B in its entirety, “Ternary blends…require retesting.”

INSERT:  The following.

Ternary blends using two SCMs and binary blends with Type IL hydraulic cement and an SCM will require C1567 testing by an accredited laboratory.  The expansion test results shall not be greater than 0.10 percent to be considered acceptable.  Changes to the SCM blend percentages will require retesting.