Category 900

MATERIALS

SECTION 912 — Coating Systems for Structural Steel

912.05 PAINT SYSTEMS.

DELETE:  In the Paint Systems Table, System H in its entirety.

INSERT:  The following for System H.

| PAINT | COAT | SECTION | DRY FILM THICKNESS, mils, min - max | USAGE |
| --- | --- | --- | --- | --- |
| SYSTEM H |  |  |  |  |
| Penetrating Sealer | I | 912.02.05 | 1.0 - 2.0 | Spot Primer/ Sealer |
| Aluminum Filled Epoxy Mastic | II | 912.02.02 | 3.0 - 5.0 | Spot Intermediate |
| Aliphatic Urethane | III | 912.04.02 | 3.0 - 5.0 | Spot Finish |